Synthesis of supported catalysts based on Co3O4 hydrosols

Mostovaya Uliana Leonidovna, Mendeleyev University of Chemical Technology of Russia, 9, Miusskaya square, Moscow, Russia, 125047, senior lecturer of analytical chemistry department, PhD, tel. +7(499) 972-44-38; e-mail: ylyana.m@gmail.ru

Gavrilova Natalia Nikolaevna, Mendeleyev University of Chemical Technology of Russia, 9, Miusskaya square, Moscow, Russia, 125047, an associate professor of colloid chemistry department, PhD; e-mail: gavrilovann@yahoo.com

Nazarov Victor Vasilievich, the head of the chair of colloid chemistry department, Mendeleyev University of Chemical Technology of Russia, 9, Miusskaya square, Moscow, Russia, 125047, PhD, professor.

Yarovaya Oxana Victorovna, Mendeleyev University of Chemical Technology of Russia, 9, Miusskaya square, Moscow, Russia, 125047, an associate professor of colloid chemistry department, PhD.

Kozlovskiy Ivan Anatolievich

Mendeleyev University of Chemical Technology of Russia,

Ph.D. in Chemistry. Chair of Technology of Base Organic and Petrochemical Synthesis. 125047, Moscow, Miusskaya sq. 9. Phone: +7(499)9789288

Keywords: hydrosols, nanoparticles Co3O4, supported catalyst, sol-gel method, oxidation of CO.

In present work samples of supported catalysts Со3О4/α-Al2O3 were synthesized with utilization of hydrosols. The morphology, specific surface and catalytic activity were investigated. It was shown that sing of Co3O4 hydrosols allows to obtain a thin catalytic layer on the particles surface of α-Al2O3, which specific surface is about 30 m2/g. It was found that coating with the help of dynamic mode is a more efficient way comparing to a multiple impregnation, and allows to increase the content of the active component by an order and to develop the specific surface of the samples in 3.5 times. Synthesized catalyst samples were tested in the reaction of CO complete oxidation. Herewith, CO complete oxidation on the samples of Co3O4 / α-Al2O3 is achieved at temperatures 250-270°С.

References

1. Lou Y., Wang L., Zhang Zh., Zhao Zh., Lu G., Guo Y. The effects of Bi2O3 on the CO oxidation over Co3O4 // Catalysis Today. 2011. V. 175. PP. 610-614.

2. Marban G., Lopez I., Valdes-Solis T., Fuertes A. Highly active structured catalyst made up of mesoporous Co3O4 nanowires supported on a metal wire mesh for thе preferential oxidation of CO // International Journal of Hydrogen Energy. 2008. V. 33. PP. 6687-6695.

3. Sun Sh., Gao Q., Wang H., Zhu J., Guo H. Influence of textural parameters on the catalytic behavior for CO oxidation over ordered mesoporous Co3O4 // Applied Catalysis, B. 2010. V. 97. PP. 284-291.

4. Zhang, Dong L.,Yu W., Liu L., Deng Y., Liu B., Wang H., Gao F., Sun K., Dong L. Effect of cobalt precursors on the dispersion, reduction, and CO oxidation of CoOx/γ-Al2O3 catalysts calcined in N2 // Journal Colloid and Interface Science. 2011. V. 355. PP. 464-471.

5. Li L., Yao Y., Tang Z., Ji W., Dai Y., Shen X. Size Effect of Co3O4 nanoparticles as catalysts for CO oxidation // Journal Nanoscience and Nanotechnology // 2016. V. 16. PP. 7573.

6. Jansson J., Palmqvist A.E.C., Fridell E., Skoglundh M., Osterlund L., Thormahlen P., Langer V. On the catalytic activity of Co3O4 in low-temperature CO oxidation // Journal Catalysis. 2002. V.211. PP. 387.

7. Krylov O.V. Geterogennyi kataliz. M.: Akademkniga, 2004. ( in Russ )

8. Xiuyan X., Jinjun L., Zhengping H. CeO2-Co3O4 Catalysts for CO Oxidation // Journal Rare Earths. 2006. V. 24. PP. 172-176.

9. Lv Y., Li Y., Shen W. Synthesis of Co3O4 nanotubes and their catalytic applications in CO oxidation// Catalysis Communications. 2013. V. 42. PP. 116-120.

10. Xie X., Li Y., Liu Z.-Q., Haruta M., Shen W. Low-temperature oxidation of CO catalysed by Co3O4 nanorods // Nature. V.458. PP. 746.

11. Yarovaya O.V., Mostovaya U.L., Nazarov V.V. Supported catalysts Co3O4/α-Al2O3 synthesis using Co3O4 nanoparticles // Khimicheskaya promishlennost segodnya [Chemical industry today]. 2014. V.7. PP. 11-19. ( in Russ )

12. Zubov V.P., Yarovaya O.V., Mostovaya U.L., Nikovskiy I.A., Lemeshev D.O.. Production of flat membrane contactors with a catalytically active Co3O4 layer / Uspekhi khimicheskoy tekhnologii [success of chemical technology]: sb.nauch. tr. 2015. V. 29. PP. 67. ( in Russ )

13. Elimelech M., Gregory J., Jia X., Williams R.A. Particle Deposition and Aggregation Measurement, Modelling and Simulation. Butterworth-Heinemann, 1995.

Express method for the analysis of C50-carotenoids of halophilic microorganisms

Murzina Ekaterina Dmitrievna

D.Mendeleev University of Chemical Technology of Russia, post-graduate student, 3 years of study, Department of biotechnology. Address: 125047, Moscow a-47, Miusskaya PL., 9 Phone 8(495)495-23-79, e-mail:katrin840@mail.ru

Butyrin Sergey Pavlovich

D.Mendeleev University of Chemical Technology of Russia, student, 4 years of study, Department of biotechnology. Address: 125047, Moscow a-47, Miusskaya PL., 9 Phone 8(495)495-23-79

Poberezhniy Daniil Yurievich

D.Mendeleev University of Chemical Technology of Russia, student, 4 years of study, Department of biotechnology. Address: 125047, Moscow a-47, Miusskaya PL., 9 Phone 8(495)495-23-79

Tumaev Michael Dmitrievich

Moscow Aviation Institute (National Research University), 1-year student, Department of automated systems of orientation and navigation. Address: 125993, Moscow, A-80, GSP-3, Volokolamskoe shosse 4. Tel. 8(499) 158-43-59

Belov Alexey Alekseevich

D.Mendeleev University of Chemical Technology of Russia, doctor of technical Sciences, associate Professor (docent), Department of biotechnology. Address: 125047, Moscow a-47, Miusskaya PL., 9 Phone 8(495)495-23-79

Suyasov Nikolay Aleksandrovich

D.Mendeleev University of Chemical Technology of Russia, candidate of technical Sciences, associate Professor (docent), Department of biotechnology. Address: 125047, Moscow a-47, Miusskaya PL., 9 Phone 8(495)495-23-79

Kuznetsov Alexander Yevgenevich

D.Mendeleev University of Chemical Technology of Russia, candidate of technical Sciences, associate Professor (docent), Department of biotechnology. Address: 125047, Moscow a-47, Miusskaya PL., 9 Phone 8(495)495-23-79

Kalenov Sergei Vladimirovich

D.Mendeleev University of Chemical Technology of Russia, candidate of technical Sciences, associate Professor (docent), Department of biotechnology. Address: 125047, Moscow a-47, Miusskaya PL., 9 Phone 8(495)495-23-79

Keywords: halophilic microorganisms, C50-carotenoids, extraction of carotenoids from biomass, carotenoids, antioxidants, bacterioruberin, Halobacterium salinarum, Halorubrum litoreum, Pseudomonas halophila.

Carotenoids have antioxidant, oncoprotective and immunomodulating activity, affect the regulation of growth and differentiation of mammalian cells. The use of carotenoids is promising for the pharmaceutical, cosmetic, food industries. Poorly studied producers of carotenoids are halophilic microorganisms, the cells of which contain various carotenoids, among which the major ones are the bacteriuruberin derivatives. The paper presents an express method for the analysis of C50-carotenoids of halophilic microorganisms, which has advantages over complex, multistage methods for their determination. The comparing between spectrophotometric and chromatographic methods of analysis has been carried ont.

References

1. Britton G., Liaaen-Jensen S., Pfander  H. Carotenoids. Volume 5: Nutrition and Health. // Boston, Berlin: Birkhauser Verlag Basel, 2009.

2. Rao A., Rao L. Carotenoids and human health // Pharmacological research. 2007.

3. Johnson E.J. The role of carotenoids in human health // Nutr. Clin. Care, 2002, v.5,  pp.56-65.

4. Koshkareva К. А., Кalenov S. V. Characteristics of the main component of the extreme halophilic community of salt crystals of lake alikes-a promising producer of carotenoids // Uspehi v himii I himicheskoy tehnologii [Journal Adnvances in Chemistry and Chemical Technology], 2016,  V. 30,  no.9,  pp. 23-24 (in Russ.).

5. Arjaev А. М. Possibilities of application of the drug baksin-vet in fur farming // Veterinariya Kubani [Kuban Veterinary], 2008 (in Russ.).

6. Rie Yatsunami, Ai Ando, Ying Yang, Shinichi Takaichi, Masahiro Kohno, Yuriko Matsumura, Hiroshi Ikeda, Toshiaki Fukui, Kaoru Nakasone, Nobuyuki Fujita, Mitsuo Sekine, Tomonori Takashina, Satoshi Nakamura / Identification of carotenoids from the extremely halophilic archaeon Haloarcula japonica // Frontiers in microbiology, 2014, vol. 5, article 100, pp. 1-5.

7. Sui Liying, Liu Liangsen, Deng Yuangao / Characterization of halophilic C50 carotenoid-producing archaea isolated from solar saltworks in Bohai Bay, China // Chinese Journal of Oceanology and Limnology, 2014, vol. 32, no. 6, pp. 1280-1287.

8. El-Sayed W.S.M., Takaishi S., Saida H., Kamekura N., Abu-Shady M., Seki H., Kuwabara T. / Effects of Light and Low Oxygen Tension on Pigment Biosynthesis in Halobacterium salinarum, Revealed by Novel Method to Quantify Both Retinal and Carotenoids // Plant Cell Physiol, 2002, vol. 43, no. 4, pp. 379-383.

9. Britton G. / General carotenoid methods //Methods in enzymology, 1985, vol. 111, pp. 113-149.

10. M. Dummer, Jessica C. Bonsall, Jacob B. Cihla, Stephanie M. Lawry, Gabriela C. Johnson, Ronald F. Peck Bacterioopsin-Mediated Regulation of Bacterioruberin Biosynthesis in Halobacterium salinarum // Journal of bacteriology, Oct. 2011, pp. 5658–5667.

Polymer compositions based on ethylene copolymers with vinyl acetate for insulating coatings of steel pipes

Kostromina Natalya Vasiljevna, Cand. Sci. (Tech.), Associate Professor of the Chair of plastics processing technology, D. Mendeleev University of Chemical Technology of Russia. Address: Miusskaya sq., 9, 125047 Moscow, Russia, 9, tel.: 8 (499) 978-97-96, e-mail: nkostromina@muctr.ru

Osipchik Vladimir Semjenovich, Dr. Sci. (Tech.), professor, professor of the Chair of plastics processing technology, D. Mendeleev University of Chemical Technology of  Russia. Address: Miusskaya sq., 9, 125047 Moscow, Russia, 9, tel.: 8 (499) 978-80-20, e-mail: vosip@muсtr.ru

Ivashkina Vera Nikolaevna, Engineer of the Chair of plastics processing technology, D. Mendeleev University of Chemical Technology of Russia. Address: Miusskaya sq., 9, 125047 Moscow, Russia, 9, tel.: 8 (499) 978-97-96, e-mail: ivashkina@muctr.ru

Aristov Vitalyj Mikhailovich, Dr. Sci. (Physic.-mathemat.), professor, Chief of the Chair of plastics processing technology, D. Mendeleev University of Chemical Technology of  Russia. Address: Miusskaya sq., 9, 125047 Moscow, Russia, 9, tel.: 8 (499) 978-82-64, e-mail: aristov@muctr.ru

Kozlovskiy Ivan Anatolievich

Mendeleyev University of Chemical Technology of Russia,

Ph.D. in Chemistry. Chair of Technology of Base Organic and Petrochemical Synthesis. 125047, Moscow, Miusskaya sq. 9. Phone: +7(499)9789288

Keywords: insulation steel pipe, copolymers of ethylene with vinyl acetate, the adhesion strength of the adhesive coating.

Domestic brands Sevilen have been actively implemented currently on the territory of the Russian Federation in the framework of import substitution, in this connection, of particular relevance has become the task of improving the quality of coatings on their basis. The article considers the properties of Sevilen mixtures with various contents of vinyl acetate used as the outer layer anti-corrosion coatings for metal steel pipe. The adhesive material for pipe insulation based on binary mixtures of ethylene-acetate copolymers has been developed. The work offers a comprehensive study of the properties of the insulating material. A significant increase in adhesive strength is observed for systems with a high level of inter-solubility of components. The protective coating obtained on the basis of copolymers of ethylene with vinyl acetate allows to receive high characteristics of adhesion strength.

References

1. Mustafin F.M. Overview of pipeline protection methods against corrosion by insulating coatings. Elektronnyj nauchnyj zhurnal Neftegazovoe Delo [The electronic scientific journal Oil and gas business], 2003, no. 1, рр. 14 (in Russ.).

2. Cherkasov N.M. Gladkikh, I.F., Filimonov, V.A., Sergeev V.I. New insulating coating for repair of main pipelines. Elektronnyj nauchnyj zhurnal Neftegazovoe Delo [The electronic scientific journal Oil and gas business], 2010, no. 1, рр. 85-89 (in Russ.).

3. Habirova A.R., Mustafin F.M., Habirov R.A. The modern state of protection of pipelines against corrosion polymer coating. Elektronnyj nauchnyj zhurnal Neftegazovoe Delo [The electronic scientific journal Oil and gas business], 2005, no. 2, рр. 2 (in Russ.).

4. Chalykh A.E., Shcherbina A.A. Polymer adhesion. Klei. Germetiki, Technologii [Adhesives. Sealants, Technologies], 2007, no. 11, рр. 2-15 (in Russ.).

5. Belov PA, Lurie S.A. Theory of ideal adhesion interactions. Mechanika kompozitsionnych materialov i konstrukziy [Mechanics of composite materials and structures], 2007, vol. 13, no. 4, рр. 519-536 (in Russ.).

Selection of adsorbent for the second stage of air separation unit by PSA method to obtain pure oxygen

Alekhina Marina Borisovna

D.I. Mendeleyev University of Chemical Technology of Russia, professor, department of technology of inorganic substances and electrochemical processes.

Address: 125047, Moscow, Miusskaya square, 9; e-mail: mbalekhina@yandex.ru

Ivanova Ekaterina Nikolaevna

D.I. Mendeleyev University of Chemical Technology of Russia, the postgraduate student.Address: 125047, Moscow, Miusskaya square, 9; e-mail: ivkatushka@gmail.com

Dudoladov Alexander Olegovich

D.I. Mendeleyev University of Chemical Technology of Russia, the postgraduate student. Address: 125047, Moscow, Miusskaya square, 9; e-mail: nerfangorn@gmail.com

Chumak Kristina Andreevna

D.I. Mendeleyev University of Chemical Technology of Russia, past master.

Address: 125047, Moscow, Miusskaya square, 9; e-mail: krischum@yandex.ru

Keywords: adsorbents, oxygen, argon, adsorption, air separation, PSA method.

Adsorbents of various types (pillared montmorillonite clays, zeolites modified with nanoparticles of transition metals, airgels based on calcium alginate and silica modified with carbon nanotubes) have been synthesized, and they have increased selectivity for argon to separate it from the mixture with oxygen. The values of the separation coefficients of argon-oxygen mixture (95 vol.% O2 and 5 vol.% Ar) were calculated as the ratio of Henry's constants and amounted to 1.1-3.9. A technique is proposed for selecting adsorbents to remove argon from its mixture with oxygen for the second stage of the oxygen production unit using the PSA method with a purity of 99% or more. At pressure values corresponding to the production and backflushing stages, the distribution coefficients of both components were calculated when adsorbed with adsorbent samples. It is shown that the best adsorbent from the samples studied is zeolite type Y, modified with silver nanoparticles.

References

1. Atroshhenko V.I. Technology of bound nitrogen. Kiev: Vishha shkola, 1985. P. 326.

2. Svit T.F. Principle of air separation by deep cooling and rectification: study guide. Barnaul: Izd-vo AltGTU, 2005. P. 132. (in Russ.).

3. Arharov A.M., Marfenina I.V., Mikulin E.I. Cryogenic systems. p. 2. Principle of designing devices, installations and systems. M.: Mashinostroenie, 1999. P. 720. (in Russ.).

4. Dytnerskij Ju.I., Brykov. V.P., Kagramanov G.G. Membrane gas separation. M.: Himija, pp. 1991. –344. (in Russ.).

5. Bondarenko V.L., Losjakov N.P., Simonenko Ju.M., Chuklin A.P., Kuz'menko I.F., Talakin O.G. Application of membrane processes in separation technologies of gas mixtures based on air components. Tehnicheskie gazy [Technical gases]. 2012 . № 2. pp. 19 – 30. (in Russ.).

6. Mishhenko M.V., Maslov V.A., Dzjubenko O.L.  Increase of economic efficiency of processes of fuel heat power plants by enriching technological air with oxygen. Sovremennye nauchnye issledovanija i innovacii [Modern scientific research and innovations]. 2011. № 7. P. 6. (in Russ.).

7. Shumjackij Ju.I. Types and principles of organization of non-heated adsorption processes for purification and separation of gas mixtures. Himicheskaja promyshlennost' [Chemical industry]. 1989. № 8. pp. 586-590. (in Russ.).

8. Shumyatskii Yu. I. Industrial adsorption processes. M: KolosS, 2009, P. 184. (in Russ.).

9. Shumjackij Ju.I. Adsorption processes with cyclic pressure changes during the adsorption and regeneration stages in the book “Adsorption, adsorbents and adsorption processes in nanoporous materials”. M.: Izdatel'skaja gruppa “Granica”, 2011. pp. 480-489. (in Russ.).

10. Kheifets L.I., Safonov M.S., Kostromitina M.B., Pavlov Yu.V., Voskresenskii N.M., Bel'nov V.K. Experimental evidence on a quasi-equilibrium model of the dynamics of adsorption of nitrogen and oxygen on NaX and CaA zeolites. Zhurnal fizicheskoj himii [Russian Journal of Physical Chemistry] A. 2002. V. 76. № 6. pp. 1009-1015. (in Russ.).

11. Bel'nov V.K., Voskresenskii N.M., Predtechenskaya D.M., Safonov M.S., Kheifets L.I. Increasing the efficiency of an air separation plant by varying the cycle stage durations. Teoreticheskie osnovy himicheskoj tekhnologii [Theoretical Foundations of Chemical Engineering]. 2007. Т. 41. № 2. pp. 143-149. (in Russ.).

12. Bel'nov V.K., Voskresenskii N.M., Kheifets L.I. Increasing the thermodynamic efficiency of an air-separating plant by recuperating the mechanical energy of the gas streams. Teoreticheskie osnovy himicheskoj tekhnologii [Theoretical Foundations of Chemical Engineering]. 2007. V. 41. № 5. pp. 519-525. (in Russ.).

13. Matvejkin V.G. i dr. Mathematical modeling and control of the short-cycle adsorption process. M.: Izdatel'stvo Mashinostroenie-1. 2007. P. 140. (in Russ.).

14.	Akulov A.K. Specialty of processes in installations of adsorption air separation. Tehnicheskie gazy [Technical gases]. 2007. № 6. pp. 39-42. (in Russ.).

15. Alehina M. B., Kon'kova T. V. Zeolites for adsorption oxygen generators. Vestnik VGU, Serija: Himija. Biologija. Farmacija [Reporter of VPU, chemistry, biology, formation line], 2011, № 2. (in Russ.).

16. Savin I.A., Kalachev M.V., Savina A.I. Analysis of laser cutting of carbon steel in oxygen medium. Nauchnyj vestnik [Scientific reporter]. 2017. № 1 (11). pp. 143-155. (in Russ.).

17. Miroshnichenko Ju.V., Enikeeva R.A., Perfil'ev A.B., Kassu E.M. A retrospective analysis of native pharmacopoeial articles on medical oxygen. Vestnik Rossijskoj voenno-medicinskoj akademii [Reporter of military medical academy]. 2017. № 1 (57). pp. 194-197. (in Russ.).

18. Kel'cev N.V. Basics of adsorption equipment. M.: Himija, 1984.- 592 s.

19. Chiang R.L., Whitley R.D., Ostroski J.E., Dee D.P. Argon/oxygen selective X-zeolite. USA 6432170, 2002.

20. Kandybin A.I., Anderson R.A., Reichley D.L. System for separation of oxygen from argon/oxygen mixture. USA 5470378, 1995

21. Knaebel K.S, Kandybin A.I. Pressure swing adsorption system to purify oxygen. USA 5226933, 1993.

22. Sebastian J., Jastra R.V. Anomalous adsorption of nitrogen and argon in silver exchanged zeolite A. The Royal Society of Chemistry. Chem. Commun. 2003. pp. 268-269.

23. Sebastian J., Jasra R.V. Sorption of nitrogen, oxygen, and argon in silver-exchanged zeolites. Ind. Eng. Chem. Res.  2005. V. 44. № 21. pp. 8014-8024.

24. Shi M. J. Kim, J.A. Sawada. Production of argon free oxygen by adsorptive air separation on Ag-ETS-10. AIChE Journal. – 2013. – Vol. 59, № 3. - pp. 982-987.

25. А. Anson., S. M. Kuznicki, T. Kuznicki. Adsorption of argon, oxygen, and nitrogen on silver exchanged ETS-10 molecular sieve. Microporous and Mesoporous Mater. – 2008. – Vol. 109, № 1-3. – pp. 577-580.

26. Ivanova E.N., Burmistrova N. N., Alekhina M. B., Dudoladov A.O., Kon'kova T.V., Maslova O.A. Modification of montmorillonite clay for the selective sorption of argon mixed with oxygen. Sorbtsionnye i khromatograficheskie protsessy [Sorption and chromatographic processes]. 2017. T. 17. № 4. pp. 657-666. (in Russ.).

27. Ivanova E.N., Burmistrova N.N., Alekhina M.B., Dudoladov A.O.  Al-pillared montmorillonite clay for selective adsorption of argon from its mixture with oxygen. Sorbtsionnye i khromatograficheskie protsessy [Sorption and chromatographic processes]. 2018. T. 18. № 1. pp. 916-926. (in Russ.).

28. Ivanova E.N., Alehina M.B., Gubajdullina G.F. Modification of zeolites with transition metal nanoparticles for the separation of argon-oxygen gas mixture. Aktual'nye problemy teorii adsorbcii, poristosti i adsorbcionnoj selektivnosti [Actual problems of the theory of adsorption, porosity and adsorption selectivity]. 2017, Moskva, Russia. pp. 133-136. (in Russ.).

29. Ivanova E.N., Burmistrova N.N., Alekhina M.B., Tsygankov P.Yu.,

Ivanov S.I. Aerogels Based on Calcium Alginate and Silicon Dioxide and Modified with Carbon Nanotubes for Selective Sorption of Argon from a Mixture with Oxygen. Zhurnal prikladnoj himii [Russian Journal of Applied Chemistry], 2017, Vol. 90, No. 10, pp. 1666−1671. (in Russ.).

30. Menshutina N.V., Katalevich A.M., Smirnova I. Synthesis of silica aerogels using supercritical drying. Sverhkriticheskie fljuidy: teorija i praktika [Supercritical Fluids: Theory and Practice]. 2013. T .8. №3. pp.49-55. (in Russ.).

31. Ivanov S.I., Cygankov P.Ju., Hudeev I.I., Men'shutina N.V. Creation of the functional material "silicon dioxide-carbon nanotubes". Uspehi v himii i himicheskoj tehnologii [Success in chemistry and chemical technology]. 2015. T. 29. № 4 (163). pp. 83-85. (in Russ.).

32. Ustinov E.A. An analysis of the equilibrium adsorption of nitrogen, oxygen, and their mixtures on zeolite NaX at temperatures of from -20 to +30°C. Zhurnal fizicheskoj himii [Russian Journal of Physical Chemistry]. 2007. Т. 81. № 2. pp. 246-254. (in Russ.).

33. Fomkin A.A. Physical adsorption of gases, vapors and liquids at high pressures on microporous adsorbents: Doctor Thesis. M., 1993. (in Russ.).

34. Abdurahmanov F.A., Patiev A.R., Alehina M.B. Adsorption of nitrogen on zeolites at elevated pressure. Uspehi v himii i himicheskoj tehnologii [Success in chemistry and chemical technology]. 2010. T. XXIY. № 9 (114). pp. 85-89. (in Russ.).

Chitosan-Containing Composites of Proteinases

Savelieva Elizaveta Evgenievna
student 4 course, Russian Chemical and Technological University. DI. Mendeleev, the Chair of biotechnology. 125480, Moscow, ul. Geroev Panfilovtsev, 20, Phone: +7 (499) 978-95-15
Dosadina Elina Eldarovna
graduate student, Royal Holloway, University of London
Brik Liliana Lyubanovna
Postgraduate Student, Chair of Industrial Pharmacy Institute of translation medicine and biotechnology of the federal state autonomous educational institution of higher education first Moscow state medical university named after im. Sechenova ministry of health of the Russian federation (Seechenovsky university)
address 119991, Moscow, ul. Trubetskaya, 8, building 2
Markvichev Nikolay Semenovich
associate professor, associate professor, Russian Chemical-Technological University named after. DI. Mendeleev, the Chair of  biotechnology,
125480, Moscow, ul. Geroev Panfilovtsev, 20, Phone: +7 (499) 978-95-15
Khanafina Anna Andreevna, student 3 course, Russian Chemical and Technological University. DI. Mendeleev, the Chair of biotechnology. 
125480, Moscow, ul. Geroev Panfilovtsev, 20, Phone: +7 (499) 978-95-15
Vanyushenkova Anna, student 2 course, Russian Chemical and Technological University. DI. Mendeleev, the Chair of biotechnology. 
125480, Moscow, ul. Geroev Panfilovtsev, 20, Phone: +7 (499) 978-95-15
Kalenov Sergey Vladimirovich
associate professor, associate professor, Russian Chemical-Technological University named after. DI. Mendeleev, the Chair of biotechnology. 
125480, Moscow, ul. Geroev Panfilovtsev, 20, Phone: +7 (499) 978-95-15
Belov Alexey Alekseevich
d.t.s., associate professor  Russian Chemical-Technological University. DI. Mendeleev, the Chair of biotechnology. 125480, Moscow, ul. Geroev Panfilovtsev, 20, Phone: +7 (499) 978-95-15; e-mail: ABelov2004 @ yandex.ru

Keywords: immobilized proteinases, chitosan, inactivation, therapeutic agent, drying, wound healing materials.

Despite the large number of developments in the treatment of purulent-necrotic wounds on the market there is still a wound healing composition satisfies the requirements of an ideal therapeutic agent. Multiple studies have established that modern wound-healing agent should possess the following properties: absorb purulent discharge and products of its destruction, to have cleansing properties (usually due to the launch of proteolytic enzyme), to have biocidal properties (especially with respect to pathogenic microflora and, first and foremost in relation to Staphylococcus aureus), as wound infection can greatly slow down the healing process, and in some cases facilitate the transition of the wound process in the chronic and include antioxidant (especially for the treatment of long-term illnesses). Development of new combined formulations of drugs requires the need for large-scale studies of the compatibility of the ingredients, the first drug substances to avoid the formation of new compounds that can alter the therapeutic effect or to result in the formation of toxic product. We studied the effect on the biological activity of the used drugs as each other, the method of receiving and drying, storing and behavior under model conditions. The calculated effective rate constants of thermal modeling in liquid medium. Obtained in the present work the results indicate a possibility of producing coimmobilized in polymer carriers of drugs proteolytic enzymes and miramistin preserving biological activity.

References

1. Khomenko A.Yu. Regulation of morphology and properties of non-woven and highly disperse biocompatible materials based on chitosan and lactic acid polymers obtained by electroforming, Diss. na sois. uchenoi step. kand.fiz-mat. nauk M., MFTI, 2016, 168 р., (in Russ.).

2. Biocompatible materials /pod red. Sevast'yanova V.I., Kirpichnikova M.P.  Moskva: Meditsinskoe informatsionnoe agentstvo, 2011, 544 р., (in Russ.).

3. Belov A.A. Development of industrial technologies for the production of new medical materials based on modified fiber-forming polymers containing biologically active protein substances Diss. na sois. uchenoi step. doktora tekhnich. nauk M., RKhTU, 2009,  385 р. , (in Russ.).

4. Ravi Kumar M. N. V., Muzzarelli R. A. A., Muzzarelli C. et al Chitosan Chemistry and Pharmaceutical Perspectives //Chem. Rev, 2004, no.104, рр.6017-6084.

5. Valérie Dodane and Vinod D. Vilivalam  Pharmaceutical applications of chitosan// PSTT 1998.Vol. 1, no. 6 September, рp.246-253.

6. Barbara Krajewska  Application of chitin- and chitosan-based materials for enzyme immobilizations: a review// Enzyme and Microbial Technology, 2004,  35, рр.126–139.

7. Hoda Jafarizadeh Malmiri, Mohammad Ali Ghaz Jahanian and Aydin Berenjian  Potential applications of chitosan   nanoparticles as novel support in enzyme immobilization// American Journal of Biochemistry and Biotechnology, 2012, 8 (4), рр.203-219.

8. Dosadina E.E.,  Brkich L.L., Pyatigorskaya N.V.  i dr.  The use of chitosan as a carrier of proteinases and miramistine for the preparation of an enzyme-containing gel. Butlerovskie soobshcheniya [Butlerov Communications],  2016, T.48, no.10, рр.49-59., (in Russ.).

9. Dosadina E.E., Belov A.A. Interaction Between Chitosan Solutions, Cellulose Carriers and Some of the Multi-enzyme Complexes  International Journal of Bioorganic Chemistry  2017, Vol.2, no.2, pp.51-60.

10.  Dosadina E. E., Kulmetyeva M.A., Belov A. A.  The changing of enzymatic activity of hydrolases immobilized on natural polysaccharide matrix for purulent and burn wounds treatment during storing and exploitation   Biointerface research in applied chemistry, 2016, v. 6, Is. 3, рр. 1291-1298.

11. Dosadina E.E., Bikineeva M.A., Evdokimenko A.Y., Savelyeva E.E., Medusheva E.O., Belov A.A. Study of interaction between chitosan and some hydrolases. Izvestiya Vuzov. Prikladnaya Khimiya i Biotekhnologiya [Proceedings of Universities. Applied Chemistry and Biotechnology]. 2017, vol. 7, no. 1, pp. 62–71 (in Russ.).

12. Belov A.A., Korotaeva A.I., Malenko O.E.  i dr. Medical materials based on modified cellulose, chitosan and polyenzyme complex  Butlerovskie soobshcheniya [Butlerov Communications],   2014, T.38 , no. 4, рр.42-47  (in Russ.).

13. Dosadina E.E., Bikineeva M.A., Evdokimenko A.Yu. i dr. Immobilization of the hydrolase of the proteolytic complex from crab hepatopancreas to certain polysaccharides - the preparation, properties, application  Butlerovskie soobshcheniya [Butlerov Communications],   2016, T.48, no. 12. рр. 83-93 (in Russ.).

14. Tarasevich B.N. IR spectra of the main classes of organic compounds / Tarasevich B.N. – M.: MGU im. M.V.Lomonosova  2012,  55р., (in Russ.).

15. Boulet-Audet M., Vollrath F., Holland C. Identification and classification of silks using infared spectroscopy  Journal of Experimental Biology  2015, Vol.218, рp.3138-3149.

16. Tap F., Majid F., Khairudin N. Structure prediction of stem bromelain from Pineapples (Ananas comosus) using procaricain enzyme as a modelling template  International Journal of Applied Engineering Research  2016,  Vol.11, рp.6109-6111.

17. Preparation of proteolytic enzymes from kamchatka crab paralithodes camchatica hepatopancreas and their application / G.N. Rudenskaya, V.A. Isaev, A.M. Shmoylov et al. // App.Biochem.Biotech. 2000, Vol.22, рp.175-184.

18. Mosolov V.V.  Proteolytic enzymes  M.: Nauka, 1971,  414 р. , (in Russ.).

19. Dosadina E.E., Savelyeva E.E., Belov A.A.   The effect of immobilization, drying and storage on the activity of proteinases immobilized on modified cellulose and chitosan  Process Biochemistry, 2018, vol. 64, January, рp.213–220.

20. Mirko Weinhold  Characterization of chitosan using triple detection size-exclusion chromatography and 13C-NMR spectroscopy thesis submitted for the degree of Dr. rer. nat. University Bremen, 2010, р.150.

21. Korchagina E.V., Philippova O.E. Multichain aggregates in dilute solutions of associating polyelectrolytes keeping a constant size at the increase in the chain length of individual macromolecules    Biomacromolecules 2010, v.11, no. 12, pp. 3457-3466.

22. Nud'ga L.A., Petrova V.A., Gofman I.V. i dr. Chemical and structural transformations in chitosan films during storage ZhPKh [J Appl Chem] 2008, T.81, Vyp.11, рр.1877-1881. (in Russ.).

23. Shipovskaya A.B., Zudina I.V.,.Fomina.V.I. i dr. New antimicrobial preparations based on the complex salt of chitosan with a chiral organic ligand  Butlerovskie soobshcheniya  [Butlerov Communications]  2015,  T.41, no.3, рр.82-94  (in Russ.).

24. Tamer M. Tamer,  Mohamed A. Hassan,  Ahmed M. Omer  et al. Synthesis, characterization and antimicrobial evaluation of two aromatic chitosan Schiff base derivatives  Process Biochemistry  2016,  Vol.51,  Iss.10, рр.1721-1730.

25. Blednov A.V. Immobilizovannye fermenty i antiseptiki v kompleksnom lechenii gnoinykh ran (Kliniko-eksperimental'noe issledovanie) Avtoreferat dissertatsii na soiskanie uchenoi stepeni kandidata meditsinskikh nauk  Minsk  2007,  p.23.

Synthesis of iron-containing nanoparticles using bacteria from lake Onego

Lyasnikova Veronika Nikolayevna, magistracy D.I. Mendeleev University of Chemical Technology of Russia; e-mail: 79104437758@ya.ru

Kalenov Sergei Vladimirovich, docent D.I. Mendeleev University of Chemical Technology of Russia; e-mail: wsezart@gmail.com

Suyasov Nikolai Aleksandrovich, docent D.I. Mendeleev University of Chemical Technology of Russia; e-mail: nik-suyasov@mail.ru

Keywords: metal nanoparticles; iron-containing nanoparticles; biosynthesis of nanoparticles; nanoparticles, lake Onego.

Synthesis of iron containing nanoparticles is rapidly developing and has many applications in medicine. Biosynthesis of iron containing nanoparticles using microbes shows great development potential in the biotechnology sector because of its advantages compared to the chemical synthesis. This study tested the bacterial capability to form iron-containing nanoparticles using bacteria from different parts of lake Onego. Throughout the course of the study eight lake water samples were grown on a special medium. To obtain the nanoparticles, we added the solution of FeCl3*6H2O into the cultures. We isolated and identified two cultures capable of producing the iron containing nanoparticles. We obtained nanoparticles from five water samples and characterized their sizes using dynamic light scattering. We also compared the sizes of the obtained particles and the size the particles in the original salt solution.

References

1. Wu W., Wu Zh., Yu T., Jiang Ch., Kim W.. Recent progress on magnetic iron oxide nanoparticles: synthesis, surface functional strategies and biomedical applications. Science and technology of advanced materials, 2015, vol. 16, no. 2, p. 023501.

2. Thakkar K.N., Mhatre S.S., Parikh R.Y. Biological synthesis of metallic nanoparticles. Nanomedicine: Nanotechnology, Biology and Medicine, 2010, vol. 6, no. 2, pp. 257-262.

3. Pantidos N., Horsfall L.E. Biological synthesis of metallic nanoparticles by bacteria, fungi and plants. Journal of Nanomedicine & Nanotechnology, 2014, vol. 5, no. 5, pp. 1000233.

4.	N.N. Filatov. Lake Onego: an atlas. Petrozavodsk, Karelskiy nauchniy tsentr RAN [Karelian Research Center RAS], 2010 (in Russ.).

5. Camacho C., Coulouris G., Avagyan V., Ma N., Papadopoulos  J., Bealer K., Madden T.L.  BLAST+: architecture and applications. BMC bioinformatics., 2009, vol. 10, no. 1, pp. 421.

The study of kinetic of cereal raw materials enzymatic processing for probiotics fermentation

Khromova Natalya Yur'evna

Third year PhD student of Department of biotechnology. Dmitry Mendeleev University of Chemical Technology of Russia.

Address: 125047, Moscow, Miusskaya sq. 9.

Phone: 8 (495) 495-23-79; e-mail: khromova-natalya@bk.ru

Karetkin Boris Alekseevich

PhD in Engineering sciences, junior research scientist of Department of biotechnology. Dmitry Mendeleev University of Chemical Technology of Russia.

Address: 125047, Moscow, Miusskaya sq. 9.

Phone: 8 (495) 495-23-79; e-mail: boris.karetkin@gmail.com

Shakir Irina Vasil'evna

PhD in Engineering sciences, associate professor of Department of biotechnology. Dmitry Mendeleev University of Chemical Technology of Russia.

Address: 125047, Moscow, Miusskaya sq. 9. Phone: 8 (495) 495-23-79; e-mail: irina_shakir@mail.ru

Panfilov Viktor Ivanovich

Grand PhD in Engineering sciences, professor, head of the Department of biotechnology. Dmitry Mendeleev University of Chemical Technology of Russia.

Address: 125047, Moscow, Miusskaya sq. 9. Phone: 8 (495) 495-23-79; e-mail: vip@muctr.ru

Keywords: pretreatment of plant raw materials, enzymatic pretreatment, cereal raw materials, probiotics, kinetics.

The combinated extraction-hydrolysis process for wheat and rye meal suspensions treatment with Protex 6L, Protex 40E or pancreatine enzymes was studied. The kinetic of formation of water-soluble peptides and amino acids was researched. It was established, that the highest process rate and final concentration of extracted proteins in solution was observed at Protex 6L enzyme preprocessing with Protex 6L enzyme both in the case of wheat meal, and in the case of rye meal. On the other hand, the highest concentration of amino nitrogen (0.25 g/L) was obtained at preprocessing with pancreatine enzyme in the both cases. The fermentations of lactic acid bacteria Lactobacillus paracasei were carried out in hydrolysates obtained, and high quality of hydrolysates for microbial nutrition was established.

References

1. Charalampopoulos D., Pandiella S.S., Webb C. Growth studies of potentially probiotic lactic acid bacteria in cereal-based substrates. Journal of Applied Microbiology, 2002, no.92, pp. 851–859.

2. Radenkovs V., Klava D., Juhnevica K. Wheat bran carbohydrates as substrate for Bifidobacterium lactis development. International Journal of Biological, Biomolecular, Agricultural, Food and Biotechnological Engineering, 2013, vol.7, no.7, pp. 605-610.

3. Novik G. I., Wawrzynczyk J., Norrlow O., Szwajcer-Dey E. Fractions of Barley Spent Grain as media for growth of probiotic bacteria. Microbiology, 2007, vol.76, no.6, pp. 902–907.

4. Holkin Yu. I. Technology of hydrolytic production. M.: Lesnaya promyishlennost, 1989, 496 p. (in Russ.).

5. Lowry O.H., Rosebrough N.J., Farr A.L., Randall R.J. Protein measurement with Folin phenol reagent. J. Biol. Chem., 1951, vol. 193, no.1, pp. 265-275.

6. MUK 4.2.2316-08. Control methods of bacteriological nutrient mediums: recommended practices. M.: Federalnyiy tsentr gigienyi i epidemiologii Rospotrebnadzora, 2008, 25 p. (in Russ.).

7. Netrusov A. I. Practicum on microbiology. M.: Akademiya. 2005, 608 p. (in Russ.).

8. Bannikova L. A. Selection of lactic acid bacteria and their application in the dairy industry. M.: Pishchevaya promyshlennost', 1975, 255 p. (in Russ.).

9. Korovin F. N. Cereals grain, grain of legumes and oilseeds. M.: Pishchevaya promyshlennost', 1964, 463 p. (in Russ.).

The effect of loading ring attachments in a column apparatus on their geometric characteristics and efficiency of heat and mass transfer

Pushnov Alexander Sergeevich,  Moscow Polytechnic University, Russia, Moscow. Phone: +7(499)187-85-16; e-mail: pushnovas@gmail.com

Bagomedov Murad Gasan-Gusenovich

Moscow Polytechnic University, post-graduate student;

e-mail: bagomedovmurad@mail.ru

Беренгартен Михаил Георгиевич

Moscow Polytechnic University, professor; e-mail: berengarten@mail.ru

Keywords: Ring attachments; ways of loading; specific surface area; porosity; equivalent channel diameter; hydraulic resistance; efficiency.

The results of the analysis of the influence of the method of loading of bulk ring attachments in a column apparatus on the main geometric characteristics of the nozzle are presented - the specific surface, porosity, equivalent channel diameter and efficiency of heat and mass transfer. Bialecki rings made of polymer materials and metal are considered as nozzles. The interaction of the geometric characteristics of the nozzle design under consideration is shown for different methods of loading into the apparatus. The advantages and disadvantages of bulk and regular loading methods are shown. The presented materials can be used in the implementation of technological calculations of column apparatuses, as well as in the development of perspective designs for contact devices.

References

1. Pushnov A.S. Gas Distribution in contact and adsorption devices with a fixed granular layer.  St. Petersburg: Publishing House of Polytechnic University, 2015. 280 p. (in Russ.).

2. Pushnov A.S. Kagan A.M. Structure and gas distribution in the column apparatus with a nozzla. Saarbrücken, deutschland: LAP Lambert Academic Publishing, 2012, 159 p.

3. Alekseev K.A. Hydrodynamics of the flow in static mixers, packed type. PhD Thesis, Kazan, 2016. (in Russ.).

4. Makhnin A.A. Improvement of processes and devices for purification of steam-air mixtures from organic solvents by sorption methods. Doctor Thesis, Yaroslavl, 2010. (in Russ.).

5. Lozova N.P. influence of height of the block of a regular nozzle on process of evaporative cooling in ventilating cooling towers. PhD Thesis, Moscow, 2013. (in Russ.).

6. Pushnov AS, Lozovaya NP, Lagutkin MG, Short-bed irrigation of the cooling tower. RU 2450231, 2011. (in Russ.).

7. Semkov K., Darakchiev S., Influence of small scale maldistribution in the vapor phase on the efficiency of rectification in packed columns / Bulgarian Chemical Communications, no. 3, pp. 42, 2010.

8. Petrashova E.N. Improvement of nozzles for separation of drops in contact devices. PhD Thesis, Moscow, 2012. (in Russ.).

9. Pushnov A.S., Lagutkin M.G., Petrosova E.N. New way regular stacking of annular nozzles for the implementation of the processes of heat and mass transfer // Chemical industry, 2010, vol. 87, no. 1, pp. 34-36. (in Russ.).

10. Pushnov AS, Petrashova EN, Lagutkin MG, New way of regular packing of the ring nozzle. RU. 2440843, 2012. (in Russ.).

11. Berengarten MG, Vitkovskaya RF, Gorodilov AA, Pushnov AS, Processes and devices for environmental protection. Packing scrubbers for contact heat exchange.  SPbGUTD, 2014, P. 82. (in Russ.).