Improving extraction technology for production of ammonium paratungstate

Giganov Vladimir Georgievich, PhD, leading researcher, Department of technology of rare elements and nanomaterials based on them. Mendeleev University of Chemical Technology of Russia, Russia, Moscow; e-mail: giganov.v@mail.ru

San Yu Aung, graduate student, Department of technology of rare elements and nanomaterials based on them. Mendeleev University of Chemical Technology of Russia, Russia, Moscow

Giganov Georgiy Petrovich, doctor of technical Sciences, Professor, Russia, Moscow

Keywords: extraction, tungsten, tertiary amines, salts of quaternary ammonium bases.

Abstract: Solvent extraction of tungsten from dilute acidic sulphate solution by salts of trialkylammonium in the presence of trialkylamine oxide has been studied. The introduction 1-2% trialkylamine oxide in the extraction system enables to eliminate the formation of the third phase in the extraction of tungsten from process solutions and improve significantly operating capacity of the extractant.

The results showed that using tertiary naphthenic amine salts allows to carry out the extraction of tungstate-ions without modifiers in the extraction system at higher  pH of aqueous phase than using salts of tertiary amines of aliphatic series.

Furthermore, application of salts of quaternary ammonium bases provide to extract selectively tungsten and molybdenum directly from alkali carbonate solutions of tungsten- containing upstream materials.

References

1.	Mkrtychyan Ya. S., Lugaj D.V., Ruban G.N. et al. Helium in Russia. Helium and its role in addressing key issues of scientific and technological progress Book 1. // Moscow, Neftegaz, 2012, 215 р. (in Russ.).

2.	Panteleev D.V., Stolypin E.V., Volchenko A.G., Syrkin A.M. Development of helium industrial production in Gazprom dobycha Orenburg, LLC // Neftegazovoe delo, [Oil and Gas Business], 2011, №2, pp. 128-135 (in Russ.).

3.	Ogrel L.D. Prospects for Russia in the helium market. // Gazovaja promyshlennost' [Gas Industry] №701, 2014, pp. 22-23 (in Russ.)..

4.	Yakutseni V.P. Helium resource base in the world and the prospects of helium industry development // Neftegazovaya Geologiya. Teoriya I Praktika. 2009, V.4, №2 (in Russ.). URL: http://www.ngtp.ru/rub/3/15_2009.pdf

5.	Saeid Mokhatab, William A. Poe, John Y. Mak. Handbook of Natural Gas Transmission and Processing, 3rd Edition Principles and Practices // Amsterdam, Gulf Professional Publishing is an imprint of Elsevier, 2015. p. 628.

6.	Conrado Rillo Millán, Leticia Tocado Martínez. U.S. Patent 8973397, 2015.

7.	Murin V.V., Kislenko N.N. et al. Technology for processing natural gas and condensate: Hand-Book: 2 vols. // Moscow, Nedra, 2002, vol. 1, p. 517 (in Russ.).

8.	Molchanov S.A., Samakaeva T.O. Complex training and processing of multi-component natural gases in the a gas chemical complexes. // Moscow, Nedra, 2013, p. 514 (in Russ.).

9.	Lapidus A.L., Golubeva I.A., Zhagfarov F.G. Gas Chemistry. // Moscow, CentrLitNefteGaz, 2008. p. 447. (in Russ.).

10.	Campbell J.M. Gas Conditioning and Processing, v.2 The Equipment Modules. 7th edition. // Campbell Petroleum Series, 1992, p. 444.

11.	Han S.A., Igoshin A.I., Kazarjan V.A., Skrjabina A.S., Sohranskij V.B. Underground storage of helium // Izhevsk, IKI, 2015, p. 272. (in Russ.).

12.	Bondarev V.L., Chugunov A.V., Sarkisova M.A.,. Bondarev Ye.V Outlooks for storing of heliumenriched natural gas in the Eastern Siberia and at the Far East // Moscow. Vesti gazovoy nauki 2015 №3(23), pp. 63-67. (in Russ.).

13.	Malbrunot, P., Vidal, D., Vermesse, J., Chahine, R., Bose, T.K. Adsorbent Helium Density Measurement and Its Effect on Adsorption Isotherms at High Pressure // Langmuir, 13 (3), 1997, pp. 539-544.

14.	Saha, D., Bao, Z., Jia, F., Deng, S. Adsorption of CO2, CH4, N2O, and N2 on MOF-5, MOF-177, and zeolite 5A. // Environ Science Technology, 2010, 44(5) pp.1820-1826.

15.	Cavenati, S., Grande, C.A. and Rodrigues, A.E Adsorption Equilibrium of Methane, Carbon Dioxide, and Nitrogen on Zeolite 13X at High Pressures // Journal of Chemical & Engineering Data, 49 (4), 2004, pp. 1095–1101.

16.	Maggs, F.A., Schwabe, P.H. and Williams, J.H. Adsorption of Helium on Carbons: Influence on Measurement of Density. // Nature, Volume 186, Issue 4729, 1960, pp. 956-958.

17.	Sirotin S.A. Technology extraction of helium concentrate. Suggestions for helium purification technology. // Scientific and Technical Council OJSC «Gazprom», Orenburg, 7-8th  September 2010 г. (in Russ.).

18.	Das, N.K., Chaudhuri, H., Bhandari, R.K., Ghosh, D., Sen, P., Sinha, B. Purification of Helium from Natural Gas by Pressure Swing Adsorption. // Current Science. 95 (12), 2008, p. 1684-1691.

19.	Dytnerskij Ju.I., Brykov. V.P., Kagramanov G.G. Membrane separation of gases. // Moscow, Himija, 1991, p. 344. (in Russ.).

20.	Nikolaev N.I. Diffusion in membranes. // Moscow, Himija, 1980, p. 232. (in Russ.).

21.	Noble R.D., Stern S.A.. Membrane Separations Technology - Principles and Applications. // Amsterdam, Elsevier, 1995, p. 738.

22.	Baker R.W. Membrane technology and applications. Second edition. //. New York, John Wiley&Sons, 2004, p. 552.

23.	Van Der Burg E., Miyagishima N., Itami Y. Spiral wound gas separation membrane module. WIPO Patent Application WO/2015/049499, 2015.

24.	Gyu Hong Min, Fufang Zha. Hollow Fiber membrane module. U.S. Patent Application 20140183123, 2014

25.	Takashi Monzen, Takahito Hirashima. Hollow-fiber membrane module. U.S. Patent 6623637, 2003.

26.	Yoji Kase, Toshimune Yoshinaga, Kenji Fukunaga, Harutoshi Hoshino. Asymmetric hollow-fiber gas separation membrane, gas separation method and gas separation membrane module. U.S. Patent 7803214, 2010.

27.	Хванг С.Т., Каммермейер К. Мембранные процессы разделения. Пер. с англ. Е.П. Моргуновой и Ю.И. Дытнерского // М.: Химия, 1981 C. 464. (in Russ.).

28.	Nicholas P. Wynn. Gas separation membrane module assembly with residue manifold. U.S. Patent 7918921, 2011.

29.	Nicholas P. Wynn, Donald A. Fulton. Gas separation membrane module assembly. U.S. Patent 7510594, 2009.

Research of thermal conductivity of composite sorption-active materials based on the zeolite and fluoric ethylene polymers

Ferapontova Lyudmila Leonidovna, researcher of laboratory № 1 of the Department of chemistry and new chemical technologies of JSC «Corporation «Roskhimzaschita». Address: 392680, Tambov, Morshanskoe shosse, 19. Phone +7 (4752) 56-06-80; e-mail: mail@roshimzaschita.ru

Grunsky Vladimir Nikolaevich, head of Department of General chemical technology at Russian Mendeleev University of Chemical Technology,  Doctor of technical Sciences. Address:125480, Moscow,  Miusskaya sq. 9. Phone +7(499) 978-90-63; e-mail:oxt2011@mail.ru

Kharitonov Nikolay Ivanovich, associate Professor of Department of General chemical technology at Russian Mendeleev University of Chemical Technology, candidate of technical Sciences. Address:125480, Moscow,  Miusskaya sq. 9. Phone +7(499) 978-90-63; e-mail:oxt2011@mail.ru

Semenov Gennadiy Mikhaylovich, Professor of Department of General chemical technology at Russian Mendeleev University of Chemical Technology, Doctor of technical Sciences. Address:125480, Moscow,  Miusskaya sq. 9. Phone +7(499) 978-90-63; e-mail:oxt2011@mail.ru

Keywords: adsorbent, a polymer matrix, thermal conductivity.

An original technique and a specially designed system which allows to measure the thermal conductivity of the sample that do not have a substantially smooth surface, were created. Osing this method the thermal conductivity of, the synthesized composite sorption-active materials (CCAY) based on the matrix of Teflon brand «F- 42B» and crystallite NaX, was measured. An analysis of the results suggests that the studied parameters is dependent on the ratio of the adsorbent-filler/polymer matrix: with an increase in CCAY binder content from 10 to 25% by weight of the thermal conductivity decreases from 0,227 to 0,184 W/(m∙K).Investigation of the secondary porous structure CCAY showed that the results are due to the increase in the transportation pores filled with air - a poor conductor of heat. It is found that the thermal conductivity of the obtained composite sorption-active materialsup to 10 - 13% higher than the mass of the zeolite NaX-B-1D.

References

1. Ferapontova L.L., Gladyshev N.F., Putin S.B. Adsorbent based on zeolite using as binder polymers of fluorinated ethylene. Himicheskaja tehnologija [Chemical Technology], 2011, T. 12, no. 4, pp. 215-222 (in Russ.).

2. Ferapontova L.L., Ferapontov Ju.A., Bulaev N.A., Putin S.B. The process for producing an agglomerated zeolite. RU № 2444404, 2012 (in Russ.).

3. Ferapontov Ju.A., Ferapontova L.L., Bulaev N.A., Putin S.B.

A method for producing a shaped sorbent. RU 2446876, 2012. (in Russ.).

4. Ferapontova L.L., Gladyshev N.F., Putin S.B. Selection of the optimal conditions for production of composite sorption-active materials based on zeolite and fluoro derivatives of ethylene. Himicheskaja tehnologija [Chemical Technology], 2012, T. 13, no. 1, pp. 11-17 (in Russ.).

5. Ferapontova L.L., Gladyshev N.F., Ferapontov Ju.A., Putin S.B. i dr. Study of physico-chemical properties of the active sorptive composite materials based on zeolite and polymers of fluorinated ethylene. Zhurnal prikladnoj himii [Journal of Applied Chemistry], 2012, T. 85, V. 3, pp. 470-476. (in Russ.).

6. Putin S.B., Ferapontov Ju.A., Ferapontova L.L., Bulaev N.A. A method for producing flexible absorbent articles. RU 2475301, 2013. (in Russ.).

7. Ferapontova L.L., Gladyshev N.F., Ferapontov Ju.A., Rodaev V.V. About the thermal stability of the composite sorption-active materials in the zeolite based fluorine derivatives and ethylene. Zhurnal prikladnoj himii [Journal of Applied Chemistry], 2013, T. 86, V. 5, pp. 844-846. (in Russ.).

8. GOST 25428-82. Teflon - 42. Specifications. M.: Izdatel'stvo standartov [standards Publishing House], 1982, р. 23. (in Russ.).

9. Balabanov P. V. The method of complex determination of thermal properties of materials. RU 2387981, 2015. (in Russ.).

10. Kel'cev V.N. Fundamentals of adsorption technology. M.: Himija, 1984. 512 p. (in Russ.).

11. Brek D. Zeolite molecular sieves. M.: Mir, 1976.781 p. (in Russ.).

Temperature influence of solvent removal at properties of composite sorption-active materials based on the zeolite and fluoric ethylene basis

Ferapontova Lyudmila Leonidovna, researcher of laboratory № 1 of the Department of chemistry and new chemical technologies of JSC «Corporation «Roskhimzaschita». Address: 392680, Tambov, Morshanskoe shosse, 19. Phone +7 (4752) 56-06-80; e-mail: mail@roshimzaschita.ru

Grunsky Vladimir Nikolaevich, head of Department of General chemical technology at Russian Mendeleev University of Chemical Technology,  Doctor of technical Sciences. Address:125480, Moscow,  Miusskaya sq. 9. Phone +7(499) 978-90-63; e-mail:oxt2011@mail.ru

Kharitonov Nikolay Ivanovich, associate Professor of Department of General chemical technology at Russian Mendeleev University of Chemical Technology, candidate of technical Sciences. Address:125480, Moscow,  Miusskaya sq. 9. Phone +7(499) 978-90-63; e-mail:oxt2011@mail.ru

Semenov Gennadiy Mikhaylovich, Professor of Department of General chemical technology at Russian Mendeleev University of Chemical Technology, Doctor of technical Sciences. Address:125480, Moscow,  Miusskaya sq. 9. Phone +7(499) 978-90-63; e-mail:oxt2011@mail.ru

Keywords: composite sorption-active materials, polymeric matrix, zeolites, solvent, temperature, secondary porosity, mechanical strength, kinetics of mass transfer processes, dynamic capacitance.

We studied the adsorption and mechanical characteristics, and characteristics of the porous structure of the secondary composite sorption-active materials (CCAY) on the basis of the zeolite and matrix of fluorinated ethylene allowed obtained under different synthesis conditions. The relationship between nature, the amount and rate of removal of the solvent on the race-stage molding and drying CCAY kinetics of mass transfer of sorbate in the cycles of sorption-desorption and resistance to mechanical stress resulting composite sorption of active materials (CCAY). It has been shown that for obtaining CCAY having high performance as a solvent for preparing a slurry for forming further advisable to use dimethylketone (acetone) at a ratio of solvent/polymer matrix of 15-30/1 ml/g. Molding the slurry adsorbent filler/ polymer matrix in acetone was necessary to carry out in the temperature range of 55-60 °C.

References

1. Ferapontova L.L., Gladyshev N.F., Putin S.B. Adsorbent based on zeolite using as binder polymers of fluorinated ethylene. Himicheskaja tehnologija [Chemical Technology], 2011, T. 12, no. 4, pp. 215-222 (in Russ.).

2. Ferapontova L.L., Ferapontov Ju.A., Bulaev N.A., Putin S.B. The process for producing an agglomerated zeolite. RU № 2444404, 2012 (in Russ.).

3. Ferapontov Ju.A., Ferapontova L.L., Bulaev N.A., Putin S.B.

A method for producing a shaped sorbent. RU 2446876, 2012. (in Russ.).

4. Putin S.B., Ferapontov Ju.A., Ferapontova L.L., Bulaev N.A. A method for producing flexible absorbent articles. RU 2475301, 2013. (in Russ.).

5. Putin S.B., Ferapontov Ju.A., Ferapontova L.L., Simanenkov Je.I.

A method for producing flexible composite sorption- active material .RU 2481154, 2013. (in Russ.).

6. Ferapontova L.L., Ferapontov Ju.A., Bulaev N.A., Putin S.B. The method for producing the absorbent element. RU 2524608, 2014. (in Russ.).

7. Ferapontova L.L., Ferapontov Ju.A., Bulaev N.A., Putin S.B. A method for producing flexible composite sorption-active materials. RU 2543167, 2015. (in Russ.).

8. Belocerkovskij G.M., Ivahnjuk G.K., Fedorov N.F., Babkin. Je.O. The basic principles of producing composite sorption-active materials. Zhurnal prikladnoj himii [Journal of Applied Chemistry], 1993, T. 66, V. 2, pp. 283-287 (in Russ.).

9. Samonin V.V., Fedorov N.F. On the question of justification of the selection of the starting components for the production of composite sorbent materials technology filled polymers. Zhurnal prikladnoj himii [Journal of Applied Chemistry], 1997, T. 70, V. 1, pp. 51-54 (in Russ.).

10. Akyil S., Eral M.J. Sorbent materials. Journal of Radioanalytical and Nuclear Chemistry 2005, V. 266, n 1, pp. 89–93.

11. Samonin V.V., Podvjaznikov M.L., Nikonova V.Ju. i dr., Sorbent materials, products, devices and processes controlled adsorption. St.Pb.: Nauka, 2009. 271 p. (in Russ.).

12. Bowie G. Keefer, Extraction and concentration of a gas component. Patent US 5082473, 1992.

13. Mamunya Ye.P., Shtompel V.I., Lebedev E.V., Pissis P., Kanapitsas A., Boiteux G. Structure and water sorption of polyurethane nanocjmposityies on organic and inorganic components. Eur. Polym., 2004, no. 10, pp. 2323-2331.

14. Ferapontova L.L., Gladyshev N.F., Ferapontov Ju.A., Putin S.B. i dr. Study of physico-chemical properties of the active sorptive composite materials based on zeolite and polymers of fluorinated ethylene. Zhurnal prikladnoj himii [Journal of Applied Chemistry], 2012, T. 85, V. 3, pp. 470-476. (in Russ.).

15. Samonin V.V., Dalidovich V.V. Study adsorption of water vapor. The kinetics of water absorption. Methodical instructions. S.Pb.: SPbGTI (TU), 1997. (in Russ.).

16. Kel'cev V.N. Fundamentals of adsorption technology. M.: Himija, 1984. 512 p. (in Russ.).

17. Brek D. Zeolite molecular sieves. M.: Mir, 1976.781 p. (in Russ.).

18. Chemical Directory. / Pod red. Nikol'skogo B.P., T.2. M:, Himija. 1964. 1168 p. (in Russ.).

Phosphorite pellets sintering processes

Bobkov Vladimir Ivanivich, The Smolensk branch of the Moscow Power Engineering Institute  (National Research University), (1 Energetichesky drive, Smolensk, 214013 Russian Federation),  ph.: +7 (4812) 65-24-33; e-mail: mail@sbmpei.ru

Keywords: sintering, roasting, modeling, pellets, heat ore preparation, phosphorus, kinetics.
This paper deals with the  phosphorite pellets sintering processes research during firing. When heated phosphorite pellets together with its hardening due to sintering a process of strength reduction  takes place because of cracks formation at carbonates thermal dissociation, followed by the appearance of new crystalline surface degradation products, as well as due to the low strength of these products themselves. The experimental obtained data  are combined well with the numerical results obtained by the proposed mathematical model.As the major factor defining structure the maintenance of carbonates which is one of the components characterizing phosphorite is accepted. The received dependences confirm influence of the maintenance of carbonates on durability of pellets. Fields of durability and calcination determine parameters of management of agglomeration, basic of which – temperature and speed of heating at the known maintenance of carbonates.

References

1. Talkhayev M.P., Borisova L.I., Sukharnikov Yu.I., Galperina S. Ya. [Proizvodstvo fosforitovyh okatyshej] Production of  pellets phosphorus. - Alma-Ata: Science, 1989. – 88p. (in Russ.).

2. Alekseev L.F., Gorbachev V.A., Kudinov D.Z., Shavrin S. V. Struktura i razrušenie okatyšej pri vosstanovlenii. [Struktura and destruction of pellets at restoration] - Moscow: Nauka Publ. [M.: Science] 1983. – 228 p. (in Russ.).

3. Goldman A.Ya. Prognozirovanie deformacionno-prochnostnyh svojstv polimernyh i kompozicionnyh materialov  [Forecasting of deformation and strength properties of polymeric and composite materials]. - L.: Chemistry, 1988. – 114p. (in Russ.).

4. Andrievsky R. A. Poroshkovoe materialovedenie  [Powder materials science]. - M.: Metallurgy, 1991.  – 118p.

5. Yershov VA., Pimenov of S. D. EHlektrotermiya fosfora  [Elektrotermiya of phosphorus]. – SPb.: Chemistry, 1996. – 80p. (in Russ.).

6. Yusfin Yu.S., Pashkov N. F., Antonenko L.K., Jacques R. M., Mayzel G. M., Bazilevich of T.N. Intensifikaciya proizvodstva i uluchshenie kachestva okatyshej [Intensifikation of production and improvement of quality of pellets]. M.: "Metallurgy", 1994. 240p. (in Russ.).

7. Soboleva V.A., Sharova V. I. Spekanie fosfatno-kremnistyh rud v oblasti temperatur izmeneniya agregatnogo sostoyaniya. V sb.: Fosfatnoe syr'e i ego termicheskaya podgotovka dlya ehlektrovozgonki zheltogo fosfora. [Agglomeration of phosphorus and siliceous ores in the field of temperatures of change of an aggregate state. On Saturday.: Phosphatic raw materials and its thermal preparation for electrosublimation of yellow phosphorus]. L.:lenniigiprokhym, 1982. – 42p. (in Russ.).

8. Bobkov V. I. Resursosbereženie v èlektrotermii pri podgotovke syrʹâ na obžigovyh mašinah konvejernogo tipa [Resource-saving in an electrothermie by preparation of raw materials on the drying cars conveyor-type]// Èlektrometallurgiâ [Electrometallurgy]. 2015, No. 7, p.26-34. (in Russ.).

9. Bobkov V. I. Issledovanie tehnologi.eskih i teplomassoobmennyh processov v plotnom sloe dispersnogo materiala [Research of technological and thermal and mass exchange processes in a dense bed of disperse material] // Teplovye processy v tehnike [Thermal processes in equipment]. 2014, No. 3, p.139-144. (in Russ.).

10. Bobkov of V. I. Intensifikaciâ processa sloevoj suški dispersnogo materiala [Intensifikation of process of  layered drying of disperse material] //Teplovye processy v tehnike [Thermal processes in equipment]. 2014. No. 9. p. 425-430. (in Russ.).

11. V. I. Bobkov, V. V. Borisov, M. I. Dli, V.P. Meshalkin. Multicriterial Optimization of the Energy Efficiency of the Thermal Preparation of Raw Materials [Multicriteria optimization of energy efficiency of technological processes of thermal preparation of raw materials]// Teoreticheskie osnovy himicheskoj tehnologii [Theoretical Foundations of Chemical Engineering]. 2015, T. 49, No. 6, p. 665-670. (in Russ.).

12. V. I. Bobkov, V. V. Borisov, M. I. Dli, V.P. Meshalkin. Modelirovanie processov obžiga fosforitovyh okatyšej v plotnom sloe [Modeling of processes of roasting the phosphorus of pellets in a dense bed]// Teoreticheskie osnovy himicheskoj tehnologii [Theoretical Foundations of Chemical Engineering]. 2015, T. 49, No. 2, p.182-188. (in Russ.).

Ammophosphate and its inwater soluble part obtained based on decomposition of off-balance phosphate ore from central kyzylkum with partially ammoniated wet-processing phosphoric acid

Ortikova Safiye Saidmambiyevna,

Institute of General and Inorganic Chemistry Academy of Sciences of the Republic of Uzbekistan, senior scientific researcher-applicant, the Laboratory of Phosphate fertilizers (100170, Tashkent, Mirzo Ulugbek str., 77-а), telephone (99871) 262-01-02; e-mail: igic@rambler.ru

Rasulov Azamjon Avazjonovich,

Namangan State University, senior teacher, department “General Chemistry”, Namangan, Uzbekistan

Telephone: (99894) 301-13-83; e-mail: igic@rambler.ru

Аlimov Umarbek Kadyrbergenovich,

Institute of General and Inorganic Chemistry Academy of Sciences of the Republic of Uzbekistan, PhD in technique, senior scientific researcher, the Laboratory of Phosphate fertilizers (100170, Tashkent, Mirzo Ulugbek str., 77-а), telephone (99871) 262-01-02; e-mail: igic@rambler.ru

Seytnazarov Atanazar Reypnazarovich,

Institute of General and Inorganic Chemistry Academy of Sciences of the Republic of Uzbekistan, Doctor of Science, leading authority, the Laboratory of Phosphate fertilizers(100170, Tashkent, Mirzo Ulugbek str., 77-а), telephone (99871) 262-01-02; e-mail: igic@rambler.ru

Namazov Shafoat Sattarovich,

Institute of General and Inorganic Chemistry Academy of Sciences of the Republic of Uzbekistan, Doctor of Sciences, Professor (100170, Tashkent, Mirzo Ulugbek str., 77-а), telephone (99871) 262-01-02; e-mail: igic@rambler.ru

Keywords: mineral mass, wet-processing phosphoric acid, ammonation, expansion coefficient, nitrogen-phosphate fertilizers, inwater soluble part, composition.

The process of ammophosphate fertilizer obtaining based on interaction of mineral mass from Central Kyzylkum phosphorite with partially ammoniated wet-processing phosphoric acid depending on the weight ratio acid: phosphate raw (from 100 : 10 to 100 : 30) and pH of acid (from 1,2 to 2,5) has been studied. The chemical composition of ammophosphate slurry and its water insoluble part have been determined. Expansion coefficient of phosphate raw material has been calculated. It is shown that the more mass fraction of phosphate raw and pH of acid, the lowest all form of phosphorus in the ammophosphate slurry. It is found out that water insoluble part of slurry contents considerable quantity of acceptable Р2О5. If relative content of acceptable phosphorus is 16,54% in 2% solution of citric acid in the initial mineralized mass, in the water insoluble part of the slurry this indication is in the range 28,46-61,87%. It has confirmed the activation of the phosphate raw material during the phosphoric acid decomposition.

References

- Shapkin M.A., Zavertyaeva T.I., Zinyuk R.Yu., Guller B.D. Double superphosphate. Technology and application. L.: Chimiya, 1987, 216 p. (in Russ.).

- Beglov B.M., Namazov Sh.S. Phosphorite from Central Kyzylkum and their processing. Tashkent, 2013. 460 p. (in Russ.).

- Suyetinov A.A., Novikov A.A., Yanishevskiy F.V., Mikayev B.T., Gabeskiriya O.V., Kuznetsova A.G., Levin V.I., Starodubtsev V.S. Research, development and application of technology of novel complex fertilizer - ammophosphate. Obzornaya Informatsiya NIITEXIM. Ser.: Mineral’nye udobreniya i sernaya kislota [Information review of SRITIER. Ser.: Mineral fertilizers and sulfuric acid], M.: NIITEXIM, 1987, 56 p. (in Russ.).

- Suyetinov A.A., Novikov A.A., Starodubtsev V.S., Mikayev B.T., Gabeskiriya O.V., Yanishevskiy F.V., Kuvshinnikova O.I. Novel development in ammophosphate technology. Obzornaya Informatsiya NIITEXIM. Ser.: Mineral’nye udobreniya i sernaya kislota [Information review of SRITIER. Ser. Mineral fertilizers and sulfuric acid], M.: NIITEXIM. 1990, 51 p. (in Russ.).

- Suyetinov A.A., Novikov A.A., Starodubtsev V.S., Gabeskeriya O.V., Levin V.I., Syrotyatnikov A.L., Kuvshinnikova O.I. Development and study of technology of phosphorus containing fertilizer – ammophosphate. Khimicheskaya promyshlennost’ [Chemical Industry], 1991, no. 9, pp. 22-24. (in Russ.).

- Starodubtsev V.S. Development and commercial introduction of phosphoric acid decomposition of Karatau phosphorite in ammophosphate technology PhD thesis. M., 1988. (in Russ.).

- Yanishevskiy F.V., Kuzmenkov A.V., Kachalkina T.P. Efficiency of direct action and consequence of ammophosphate obtained from different kind of phosphate raw (field experiment results). Agrokhimiya [Agrochemistry], 1999, no. 6, pp. 35-41. (in Russ.).

- Suyetinov A.A., Levin V.I., Gabeskiriya O.V., Mikayev B.T. Recommendation on output, application and reconstruction of manufactures on chemical industry. Issue 1, 1987, 51 p. (in Russ.).

- Alimov U.K., Ortikova S.S., Abasov X.K., Namazov Sh.S., Ammophosphate based on partially ammoniated wet-processing phosphoric acid and off-balance from Central Kyzylkum phosphorite. Khimicheskiy Jurnal Kazaxstana [Chemical Journal of Kazakhstan], 2015, no. 5, pp. 12-18. (in Russ.).

- Ostanin A.I. Agrochemical foundation of production and application of phosphoric fertilizers with low solubility: Doctor Thesis. M., 1987. (in Russ.).

- Yanishevskiy F.V., Malonosova I.A., Sennitskaya L.I., Brodskiy A.A., Chelebi G.A., Murashova S.K. Agrochemical efficiency of ammophosphate on black earth and sierozem soils. Agrokhimiya [Agrochemistry], 1987, no. 10, pp. 32-41. (in Russ.).

- Vinnik M.M., Erbanova L.N., Zaytsev P.M., Ionova L.A., Makarevich V.M., Nepomnyashcaya N.A., Osherovich R.Kh. Methods of analysis of phosphate raw, phosphorus and complex fertilizers, feed phosphates M.: Chimiya, 1975, 218 p. (in Russ.).

- Lapina L.M., Grishina I.A., Usacheva N.I., Portnova N.L. On character of compounds, forming during the neutralization by ammonia of phosphoric acid, containing aluminum and iron. Jurnal prikladnoy chimii [Journal of applied chemistry], 1972, no. 1, pp. 6-11. (in Russ.).

- Brutskus Ye.B., Litsova A.I., Portnova N.L. Composition of precipitates, forming during the ammonization of phosphoric acid, containing iron and aluminum. Tr. NII po udobreniyam i insektofungitsidam [Proceedings of SRI on fertilizers and insecticide- fungicide]. M. 1973, Issue 221, pp. 35-45. (in Russ.).

- Kononov A.V., Trutneva N.V., Leneva Z.L., Yevdokimova L.M. Amount and composition of solid phase, forming during the ammonization of wet-processing phosphoric acid from order raw of Karatau in a range pH 1.3-2.5. Khimicheskaya promyshlennost’ [Chemical Industry], 1983, no. 7, pp. 417-419. (in Russ.).

- Portnova N.L., Klenitskiy A.I., Kononov A.V. Reaction flowing during the ammonization of wet-processing phosphoric acid. Deponirovanniy v ONIITEXIM. Cherkass, №3275G'79 dep., [Deposited in ONIITEXIM] M.: NIUIF, 1979, 9 p. (in Russ.).

Noncaking ammonium nitrate with the addition of bentonite clay from navbahor and lagon deposit

Turdialiev Umid Muhtaralievich,

Institute of General and Inorganic Chemistry Academy of Sciences of the Republic of Uzbekistan, senior scientific researcher, the Laboratory of Phosphate fertilizers (100170, Tashkent, Mirzo Ulugbek str., 77-а), telephone (99871) 262-01-02;

e-mail: eco-planning@mail.ru

Namazov Shafoat Sattarovich,

Institute of General and Inorganic Chemistry Academy of Sciences of the Republic of Uzbekistan, Doctor of Sciences, Professor (100170, Tashkent, Mirzo Ulugbek str., 77-а), telephone (99871) 262-01-02; e-mail: igic@rambler.ru

Reymov Ahmed Mambetkarimovich,

Institute of General and Inorganic Chemistry Academy of Sciences of the Republic of Uzbekistan, Doctor of Science, Deputy of scientific study  (100170, Tashkent, Mirzo Ulugbek str., 77-а), telephone (99871) 262-01-02; e-mail: igic@rambler.ru

Seytnazarov Atanazar Reypnazarovich,

Institute of General and Inorganic Chemistry Academy of Sciences of the Republic of Uzbekistan, Doctor of Science, leading authority, the Laboratory of Phosphate fertilizers (100170, Tashkent, Mirzo Ulugbek str., 77-а), telephone (99871) 262-01-02; e-mail: igic@rambler.ru

Beglov Boris Mihaylovich,

Institute of General and Inorganic Chemistry Academy of Sciences of the Republic of Uzbekistan, Academician  (100170, Tashkent, Mirzo Ulugbek str., 77-а), telephone (99871) 262-01-02; e-mail: begloff@mail.ru

Keywords: ammonium nitrate, bentonite, melt, strength of granules, caking, the thermal stability, rheological properties.

The process of noncaking ammonium nitrate by the addition of bentonite from Navbahor and Lagon into the melt of ammonium nitrate (99.85% solution) before granulation has been studied. Amount of bentonite was changed from 0.5 to 3g towards to 100g of ammonium nitrate melt. The composition and properties (strength granules, caking, the dissolution rate of the granules, heat resistance) of the resulting products have been determined in this study. Rheological properties of the nitrobentonite melt in the range of temperatures of 170-185oС have been investigated. Reduction of caking, increasing of strength and stability of the fertilizer granules to termal cycles of heating and cooling are results of the present study. It is shown that mixing of ammonium nitrate melt with powder bentonite with subsequent granulation slurry in the granulation tower allows to obtain the qualitative nitrogen fertilizers with improved physico-chemical and agricultural chemistry characteristic.

References

1.	Ivanov M.E., Olevskiy V.M., Polyakov N.N., Strijevskiy I.I., Ferd M.L., Tsehanskaya Yu.V. Technology of ammonium nitrate. M.: Chimia, 1978. 312 р. (in Russ.).

2.	Polyakov N.N., Nizyaev V.M., Kantor A.S., Vasyutin M.N., Basova R.P., Kondrasheva V.P., Kambulova L.D., Olevskiy V.M. A method of obtaining granular ammonium nitrate. RU 426451, 1974 (in Russ.).

3.	Polyakov N.N., Kantor A.S, Grishaeva O.S. Stabilizing action phosphate-sulphate additive on ammonium nitrate melt during the evaporation // Azotnaya promyshlennost’ [Nitrogen industry], 1974, no.3, pp.15-17. (in Russ.).

4.	Brown M.L., Green A.W., Blanton E.L. Journal Agr. Food Chem., 1968, v.16, no. 3, pp. 373-377.

5.	Abrosimova A.M., Golius L.M., Shinkorenko P.K., Zelenskaya N.M., Muzhchill’ L.I., Fedorov A.N., Lyulyushina O.A., Kirindasova R.Ya., Shevtcov A.E., Polyakov N.N. A method of obtaining granular ammonium nitrate.RU 525652. no. 31, 1976. (in Russ.).

6.	Fridman S.D., Skum L.S., Demchenko V.A., Kirindasova R.Ya., Dubova V.N., Belyaeva N.N. Obtaining and property of granular ammonium nitrate with bentonite additive// Trudy Gosudarstvennogo nauchno-issledovatel’skogo i proektnogo instituta azotnoy promyshlennosti [Proceedings of State scientific and research and project institute of nitrogen industry], 1974, Issue 24, pp. 15-21. (in Russ.).

7.	Avliyakulov A., Tungushova D., Slesareva L.S. Application agriculture ore under the cotton // Selskoe khozyaystvo Uzbekistana [Agriculture of Uzbekistan] // 2003, no. 9, pp. 15. (in Russ.).

8.	Vinnik M.M., Erbanova L.N., Zaytsev P.M., Ionova L.A., Makarevich V.M., Nepomnyashcaya N.A., Osherovich R.Kh. Methods of analysis of phosphate raw, phosphorus and complex fertilizers, feed phosphates M.: Chimia, 1975, 218 p. (in Russ.).

9.	GOST 30181.4-94. Mineral fertilizer. Method of determination of overall and mass fraction of nitrogen containing in the complex fertilizers and nitrates in ammonia and nitrate forms (Devarde’s method) (in Russ.).

10.	GOST 21560.2-82. Mineral fertilizer. Test method. M.: Gosstandart, 1982, 30 p. (in Russ.).

11.	Olevskiy V.M., Polyakov N.N.. Results of industrial tests of ammonium nitrate for packing and friability // Referativniy sbornik «Azotnaya promyshlennost’» [Abstract collection «Nitrogen industry»]. – M.: NIITEHKHIM, 1974, s. 6-8. (in Russ.).

12.	Chyorniy V.A., Streltsov O.A. Aerforce application for modification of nitrogen containing fertilizers// Khimicheskaya tekhnologiya [Chemical industry], 1988, no 2, pp. 47-49. (in Russ.).

The algorithm and computer program for synthesis of complex water treatment systems

Orlov Nikolay Savelyevich, D. Mendeleev University of Chemical Technology of Russia, Department of membranen technology (12504,  Miusskaya pl. 9 Moscow, Russia).   Tel. +7(499) 978- 36- 02; e-mail: info@steripore.ru

Keywords: chemical-engineering system, integrated purification system, methodology, synthesis procedure, technical-and-economic criteria, membrane processes.

The algorithm regulates the sequence of actions aimed at the synthesis of technological schemes of water treatment systems, and technical-and-economic calculation of size, price and operating costs of the main equipment. In solving the problem of topology of processes in the water purification system as the defining parameters of the flow condition we consider the composition and the concentration of impurities. These composition and concentration of impurities is purposely changed on the way from the point of water intake to the final stage of water treatment process, in accordance with regulatory requirements of the quality of purification process. The solution of the feasibility study that implies the choice of a "gentle" modes of operation of equipment is illustrated by the calculation of reverse osmosis. We look at the examples of the synthesis of technological schemes and of the computation of the equipment based on the computer program.

References

1. Kafarov V.V., Dorohov I.N., System analysis of processes of chemical technology. // MSK: Science, 1976,  pp 449.

2. Nalyetov A.U., Principles of creation of resource-saving environmentally sound technological schemes, dissertation, Tch.D, MSK, 1993.

3. Orlov N.S.  Methodology for the development of integrated systems of purification of liquid References: media technology based processes baromembrane, Tch.D., M, 2000, p.405 (in Russ.).

4. Orlov N.S. Primenenie noveyshix memdrannych texnologiy v promyshennosti  i ekologii Liquid-phase membrane systems for medicine, biotechnology, food, etc. Industries. [Use of the latest membrane technology in the industry and the environment], M., 1997, pp. 17-22.

5. Gartman T.N., Sowetin F.S. Analititicheskiy obzor sovremennux paketow modeliryuchix program dla komputernogo modelirovania chimiko-technologicheskix system.[ An analytical review of modern simulation software packages for computer modeling of chemical processes // Advances in chemistry and chemical technology,  2012. - №11, p.140.

6. Gartman T.N., Sowetin F.S., Losev W.A., Drobyshevskiy N.A.,   Khvorostyanov V.S. Development of a computer model of a multi-stage production of synthetic liquid fuels from natural gas // Chemical industry today, 2009. - №1, pp.40-50.

7. DOW ROSA v.9.1 Filmtec membranes ROSA help : http://dowwater.custhelp. com/app/answers/detail/a_id/205/kw/rosa/session/L3RpbWUvMTQwMjgzND cxMS9zaWQvRFBUNmdUV2w%3D.

8. GE WinFlows v.3.3.2: http://www.gewater.com/resources/winflows

9.Orlov N.S., Kuznetsova I.K., Borodkin A.G. Comparison of different channel constructions and their efficiency in membrane cells.// Desalination. – 1991.-v.81, №4, P.223-224

10. Kuznetsova I.K., Orlov  N.S., Borodkin A.G. Impact separators efficiency of mass transfer in membrane channels. Сhimicheskaya tehnologiya [Chemical technology], 2000, no. 5, pp.117-120 (in Russ.).