**Strategic directions of development of the petrochemical industry in Russia**

**Vazhenina Larisa Vitaljevna***,* Tyumen state oil and gas University, *candidate of economic Sciences*, *associate Professor; e-mail:* *Vagenina@rambler.ru*

**Keywords:** strategy, petrochemical industry, efficiency, hydrocarbon processing, food processing.

The significant part of the oil producing countries , has конецформыначалоформыpoorly developed their own process industry. Prompt reduction of stocks of oil (the peak of world extraction will be passed by 2020) and unstable pricing forces these countries to search for alternative sources of the income. Last time more and more attention is paid to natural gas, including casing-head gas and even to industrial emissions. Due to the fact that oil is not renewable resource in the oil companies the process of diversification has begun. The strategic purpose of the world oil corporations become intensive development of gas sector, integration into electric power industry, coal branch and transformation finally into the power companies. Oil gas extracting and petrogaschemistry gradually pass in the category of hi-tech branches. In modern conditions the hydrocarbon processing industry requires a dynamic and innovative development which is impossible without creating your own advanced technologies. As a strategic product directions of development of hydrocarbon processing it is reosonableto consider those that are at the junction of the priorities of different sectors and have a synergistic multiplier effect.

**References**

1.Bitumen: a derelict refinery. Neftegazovaya vertical [Oil and gas Vertical], 2015, no.1, pp. 1-5 (in Russ.).

2. Vazhenina L.V. Poputnyi Neftyanoi Gaz: Opyt Pererabotki i Otsenka Effektivnosti [Associated petroleum gas: the experience of processing and evaluating the effectiveness], Tyumen’, 2011 (in Russ.).

3. Vazhenina L.V. Napravleniya povysheniya Energoeffektivnosti v magistral’nom transporte gaza [Directions of increase of efficiency in pipeline transport of gas], Tyumen’, 2012 (in Russ.).

4. Vazhenina L.V. Ekonomika prirodopol’zovaniya [Environmental economics], Tyumen’, 2007 (in Russ.).

5. Vazhenina L.V. Ekonomika i upravlenie proizvodstvom na predpriyatiyah neftegazohimii i neftepererabotki [Economics and production management at the enterprises of the petrochemical and refining], Tyumen’, 2014 (in Russ.).

6. State program of the Russian Federation «Energy Efficiency and development of energy». Postanovlenie Pravitel’stva RF [Government Decree of the Russian Federation], 15.04.2015. no. 321 (in Russ.).

7. Refining under the flags of modernization. Neftegazovaya vertical [Oil and gas Vertical], 2014, no. 23-24, pp. 70-80 (in Russ.).

8. Energy in Russia: problems and prospects. Trudy Nauchnoi sessii RAN [Proceedings of the Scientific session of the Russian Academy of Sciences], 2006 (in Russ.).

9. Energy strategy of Russia for the period up to 2030. Prilozhenie k Energeticheskaya politika [Application Energy policy], 2010 (in Russ.).

**Iron-contained catalysts based on aluminum and silicon oxides for the oxidative degradation of azo dyes in aqueous phase**

**Kon’kova Tatiana Vladimirovna**

D.I. Mendeleyev University of Russia

Department of Technology of Inorganic Substances

125480, Moscow, 20 Geroev Panfilovtsev str. E-mail: kontat@list.ru

**Gordienko Mariia Gennadievna**

D.I. Mendeleyev University of Russia

Science-research department

125480, Moscow, 20 Geroev Panfilovtsev str. E-mail: mariya.gordienko@gmail.com

**Alekhina Marina Borisovna**

D.I. Mendeleyev University of Russia

Department of Technology of Inorganic Substances

125480, Moscow, 20 Geroev Panfilovtsev str. E-mail: mbalekhina@yandex.ru

**Menshutina Natalia Vasilievna**

D.I. Mendeleyev University of Russia

International Science and Education Center for Transfer of Biopharmaceutical technologies

125480, Moscow, 20 Geroev Panfilovtsev str. E-mail: chemcom@muctr.ru

**Keywords:** catalysts, aluminum oxide, silicon oxide, sol-gel method, oxidative degradation of dyes

Iron-contained catalysts based on mesoporous aluminum and silicon oxides prepared by the sol-gel method with gelation in acid and alkaline medium had shown high efficiency in response to oxidative degradation of azodye carmoisine in aqueous solutions. Results of stability study on catalysts to leaching of iron ions in the solution during catalysis had shown that the most stable catalysts, carriers which were obtained by gelation in an acid medium. Sample of the catalyst based on aluminum oxide had the highest stability, which is explained by the formation on the surface of highly dispersed phase of α-Fe2O3. Fe-containing catalysts based on alumina and alumina-silica gels with biporous structure are promising materials for wastewater cleaning from the impurities of organic dyes.

**References:**

1. Rodionov, A. I. Klushin, V. N., Sister V. G. Technological processes of ecological safety. Kaluga: Izdatelstvo N.F. Bochkareva [Kaluga: Publishing house N. F.Botchkareva], 2007, 800 p.(in Russ).

2. Krasnoborodko I.G. Destructive purification wastewater from dyes. L. Himiya [L.: Chemistry], 1988, 192 c. 3.Liotta L. F. Gruttadauria M., Carlo G. D. (in Russ)

3.Heterogeneous catalytic degradation of phenolic substrates: Catalytic activity. Journal of Hazardous Materials, 2009, v. 162, pp. 588-606.

4.Navalon S., Alvaro M., Garcia H. Heterogeneous Fenton catalysts based on clays, silicas and zeolites . Applied Catalysis B: Environmental, 2010, v. 99, pp. 1-26.

5. Soon A. N., Hameed B. H. Heterogeneous catalytic treatment of synthetic dyes in aqueus media using Fenton and photo-assisted Fenton process. Desalination, 2011, v. 269, pp. 1-16.

6. Kudryavtsev A.A. Compilation of chemical equations. M.: Vysshaya shkola, 1991, 320 p.

7. Atheel H.A., Ahmad Z.A., Norli I. Zeolite Y encapsulated with Fe-TiO2 for ultrasound-assisted degradation of amaranth dye in water. Journal of Hazardous Materials, 2012, v. 233-234, pp. 184-193.

8. Najjar W., Azabou S., Sayadi S., Gourbal A. Screening of Fe-BEA catalysts for wet hydrogen peroxide oxidation of crude olive mill wastewater under mild conditions. Applied Catalysis B: Environmental, 2009, v.88, pp.299-304.

9. Martins M.D.R.S., Martins A., Alegria E.C.B.A., Carvalho A.P., Pombeiro A.J.L. Efficient cyclohexane oxidation with hydrogen peroxide catalysedby a C-scorpionate iron(II) complex immobilized on desilicated MOR zeolites. Applied Catalysis A: General, 2013, v. 464– 465, pp. 43– 50.

10. Nezamzadeh-Ejhieh A., Amiri M. CuO supported clinoptilolite towards solar photocatalytic degradation of p-aminophenol. Powder Technology, 2013, v. 235, pp. 279–288.

11.Chen Y., Li G., Yang F., Zhang S.M. Mn/ZSM-5 participation in the degradation of cellulose under phosphoric acid media. Polymer Degradation and Stability, 2011, v. 96, pp. 863-869.

12. Sum O.S., Feng J., Hu X. Pillared laponite clay-based Fe nanocomposites as heterogeneous catalysts for photo-Fenton degradation of acid black 1. Chemical Engineering Science, 2004, v. 59, pp. 5269-5275.

13. Hassan H., Hameed B.H. Fe-clay as effective heterogeneous Fenton catalyst for the decolorization of Reactive Blue 4. Chemical Engineering Journal, 2011, v. 171, no. 3. pp. 912-918.

14. Daud N.K., Hameed B.H. Acid Red 1 dye decolorization by heterogeneous Fenton-like reaction using Fe/kaolin catalyst. Desalination, 2011, v. 269, pp. 291-293.

15. Virkutyte J., Varma R. S. Photoinduced catalytic adsorption of model contaminants on Bi/Cu pillared montmorillonite in the visible light range. Separation and Purification Technology, 2011, v. 78, pp. 201-207.

16. Zhong X., Barbier J., Duprez D., Zhang H., Royer S. Modulating the copper oxide morphology and accessibility by using micro-mesoporous SBA-15 structures as host support: Effect on the activity for the CWPO of phenol reaction. Applied Catalysis B: Environmental, 2012, v. 121– 122, pp. 123– 134.

17. Adam F., Andas J., Rahman I.A. A study on the oxidation of phenol by heterogeneous iron silica catalyst. Chemical Engineering Journal, 2010, v. 165, pp. 658-667.

18. Muthukumari B., Selvam K., Swaminatham M. Photoassisted hetero-Fenton mineralization of azo dyes by Fe(II)-Al2O3 catalyst. Chemical Engineering Journal, 2009, v. 153, pp. 9-15.

19. Munoza M., Pedroa Z., Menendezb N., Casasa J., Rodrigueza J. J. A ferromagnetic γ-alumina-supported iron catalyst for CWPO. Application to chlorophenols. Applied Catalysis B: Environmental, 2013, v. 136– 137, pp. 218– 224.

20. Pat. Russian Federation № 2301790. The process for the oxidation of organic compounds in the presence of hydrogen peroxide (options). ( in Russ)

21. Alekhina M.B., Papkova M.V., Kon'kova T.V., Kutepov B.I. Catalysts based on NaY zeolite for oxidative destruction of organic azo dyes in wastewater Iurnal Prikladnoi Chimii.[ Russian Journal of applied chemistry], 2013, v. 86. no. 11, pp. 1741-1745.

22. Neimark I.E. Synthetic mineral sorbents and carriers of catalysts // Kiev: Naukova Dumka [Kiev: Naukova Dumka], 1982, 216 p. ( in Russ)

23. Lim H., Lee J., Jin S. Kim J. Highly active heterogeneous Fenton catalysts using iron oxide nanoparticles immobilized in alumina coated mesoporous silica. Chemical Communication, 2006, pp. 463-465.

**The composition and structure of the polymer-nickel coatings produced by electrodeposition on the cathode**

**Romanova Olga** A. MUCTR , postgraduate major chemistry and technology polymeric film-forming materials, e-mail: olga.rhtu@yandex.ru

**Silaeva Anna A**., MUCTR , postgraduate major chemistry and technology polymeric film-forming materials; e-mail: silushka92@mail.ru

**Kvasnikov Mikhail** Yu. MUCTR, professor major chemistry and technology polymeric film-forming materials; e-mail:kvasnikovm@mail.ru

**Utkina Irina** F. MUCTRengineer major chemistry and technology polymeric film-forming materials; e-mail: silushka92@mail.ru

**Antipov Eugene** M. MUCTR,professor, chief major chemistry and technology polymeric film-forming materials; e-mail: emantipov@gmail.com

**Korolyov Yuri** M. A.V.Topchiev Institute of Petrochemical Synthesis, RAS; e-mail: korolev@ips.ac.ru

**Keywords**: metal-coating polymer electrolytes, gel fraction, intermetallic, X-ray analysis.

In order to improve the functional capacity of this method we proposed to combine cathodic electrodeposition of polyelectrolytes with electroplating. Using the modern methods of physical and chemical analysis, as well as the method of extraction of oligomer with sutable solvent we studied composition and structure of a layered coatings obtained by electrodeposition on the cathode amine polyelectrolyte together with nickel electroplating. We proposed the mechanism of coatings formation and causes of shown properties that differ significantly from the properties of the coatings from the initial systems, namely high microhardness with consistently good elasticity and an order of magnitude higher corrosion resistance. We found that in the process of electrodeposition in the initial period of time intermetallic iron-nickel is formed, which causes the manifestation properties, as well we found the catalytic effect of nickel on the process of curing.

**Reference**

1. Krylova I.A. Painting by electrodeposition on the eve of the 21st century // Progress in Organic Coating, 2001. Vol.42, pp.119-131.
2. Kvasnikov M. Ju., Utkina I.F. Krylova I.A., Romanova O.A., Smirnov K.N. Preparation of metal-coating combination in a process of electrodeposition of metals with a cathodic electrodeposition waterborne oligomeric polyelectrolyte //Chimicheskaya promyshlennost’ segodnya, [Chemical industry today], 2014.№2. pp.51-56(in Russ).
3. Kvasnikov M. Ju., Utkina I.F., Krylova I.A., Romanova O.A., Smirnov K.N., Kiselev M.R., Zolotarevskii V.I. Structure and properties of metal-polymer coatings obtained by a combination in situ process of electrodeposition of metals with cathodic electrodeposition of waterborne oligomeric polyelectrolyte // Chimicheskaya promyshlennost’ segodnya, [Chemical industry today], 2014. № 3. pp. 39-46. (in Russ).
4. Roldugin V.I. Quantum-metal colloidal systems // Uspehi Chimii, [Russian Chemical Reviews], 2000. №10. pp.897-924. (in Russ).

Mikheev V.I. Radiographic determinant of minerals. M: Gos. Nauchno-tehnich. Isd-vo literatury po geologii i ohrane nedr. [St. Scientific and Technical. Publishing House of the literature on the geology and protection of subsoil], 1957 (in Russ).

**Electrochemical synthesis in Russia. Status and prospects**

**Tomilov Andrew Petrovich,**  the Chief researcher of the State SCIENTIFIC RESEARCH INSTITUTE of organic chemistry and technology (Gosniiokht), doctor of technical sciences, Professor; e-mail: harlamova\_tanya@list.ru

**Kharlamov Tatyana Andreyevna**, professorof Moscow Mountain State University; e-mail: harlamova\_tanya@list.ru

**Keywords:** electrolysis, electroorganic synthesis, electrolyzer, emulsion, nonaqueous solvents, initiation of chain reactions.

Fifty-year experience of testing and technological implementation of both large- and small-scale productions of electroorganic synthesis is summed up. The ways of improving the technical-and-economic parameters of electrolysis are considered by certain examples. It is shown that the use of non-diaphragm (one-electrolyte) electrolyzers is most rational for commercial-scale productions of fine organic synthesis. Considerable positive effect can be achieved with electrolysis of two-phase systems – emulsions, and properly organized mass transfer in the interelectrode space is of paramount importance. Gas-lift circulation is efficient for one-phase electrolytes. The processes described were tested industrially or on pilot scale. Advanced processes with the use of nonaqueous solvents are presented. Of particular interest is recently disclosed electrochemical initiation of chain reactions which allow the electrical energy consumption to be reduced by a factor of several tens. The article may be useful in working out novel processes of electrochemical synthesis.

**References**

1. Lund H. A Century of Organic Electrochemistry. J. Electrochem. Soc., 2002, v. 149(4), pp. 21-32.

2. Tomilov A.P. Development of domestic electrochemistry of organic compounds (1940-2002). Rossiiskii himicheskii zhurnal [Russian Journal of Chemistry] 2005, v. 49, no. 5, рр. 4- 16 (in Russ.)

3. Tomilov A.P. Development of electrochemical synthesis of organic compounds in Russia in ХХ сentury. Himicheskaia promyshlennost [Chemical Industry], 2002, no. 10, pp.23-32(in Russ.)

4. Berezovskii V.M., Varkov V.S. Electrolytic reduction of galoalkyl-substituted aromatic nitrocompounds. Zhurnal obshchei himii [Journal of general chemistry], 1953, v. 23. pp. 100- 104(in Russ.)

5. Freidlin G.N., Kovsman E.P., Adamov A.A., et al. Development of the electrochemical manufacture of sebacic acid. Study of electrosynthesis of diesters of dicarboхylic acids. V kn.: Elektrosintez monomerov. Pod red. L.G. Feoktistova [In: Electrosynthesis of monomers. Edited by L.G. Feoktistova] M, Nauka, 1980, pp. 28-73 (in Russ.)

6. Kamneva L.I., Mirkind L.A., Fioshin M.Ya. Electrochemical synthesis of highest unsaturated dicarboхylic acids. Himicheskaia promyshlennost [Chemical Industry], 1966, no. 11, pp. 804-809 (in Russ.)

7. Tomilov A.P., Osadchenko I.M. Electrochemical synthesis of 2,3-dimethylbutanediol-2,3. Himicheskaia promyshlennost [Chemical Industry], 2000, no. 10, pp. 544-548) (in Russ.)

8. Tomilov A.P.. Klimov V.A., Harlamova T.A. Further development of adipodinitrile electrosynthesis. Himicheskaia promyshlennost [Chemical Industry], 1980, no. 4, pp. 200-204 (in Russ.)

9. Varshavskii S.L., Kulikov M.G., Smirnov Yu.D., Tomilov A.P. Electrochemical synthesis of heхamethylenediamine and aminocapronitrile. Himicheskaia promyshlennost [Chemical Industry], 1965, no. 5, pp. 329-332 (in Russ.)

10. Yuzbekov Yu.V., Shabaev N.B., Tomilov A.P., et al. Electrochemical synthesis of dichloroethane – a novel way of utilization of secondary hydrochloric acid. Himicheskaia promyshlennost [ Chemical Industry], 1991, no. 1, p. 14-18 (in Russ.)

11. Ignat’ev N.V., Datsenko S.L., Nechitailo L.A. Electrochemical synthesis of flouroorganic compounds. V kn.: Novosti elektrohimii organicheskih soedinenii`. Tezisy dokladov XII soveshchaniya EKHOS [In book: News of Electrochemistry of organic coumpounds. Heads of reports of XVII ECHOC conference] M., Karaganda, 1990, p. 110 (in Russ.)

12. Andruseva S.I., Kovsman E.P., Freidlin G.N., Goncharov V.N. The Behavior of electrolysis system under condition of electrosynthesis of titanium alcoholates. V kn.: Novosti elektrohimii organicheskikh soedinenii. Tezisy dokladov XII soveshchaniya EKHOS [In book: News of Electrochemistry of Organic compaunds. Heads of reports XVII conference ECHOC]. M., Karaganda, 1990, p.45 (in Russ.)

13. Islamgunova V.R., Shitova E.N., Tomilov A.P. Electrochemical synthesis of azodicarbonamide. Zhurnal prikladnoi himii [Journal of Applied Chemical ], 1998, v. 70, no. 7, pp. 1126-1131(in Russ.)

14. Osadchenko I.M., Tomilov A.P. New electrochemical process – synthesis of EFAL-50. Himicheskaia promyshlennost [Chemical Industry], 1995, no. 10, pp. 612- 614 (in Russ.)

15. Smirnov Yu.D., Shitova E.N., Shaidulina G.F., Tomilov A.P. New electrochemical process – synthesis of EDIL. Himicheskaia promyshlennost [Chemical Industry], 1996, no.2, pp. 277-281 (in Russ.)

16. Avrutskaia I.A., Fioshin M.Ya., Borisov D.I. Electrochemical oхidation of sugars. V kn.: Itogi nauki. Elektrohimiia [In book: Resume of science. Electrochemistry], 1969, M.: VINITI, 1971, v. 6, pp. 239-245(in Russ.)

17. Fioshin M.Ya., Avrutskaia I.A., Mulina G.E. Electrosynthesis diacetoneketogulonic acid on nickel oхide electrode. Elektrohimiia [Electrochemistry], 1973, v. 9, no.6, pp. 897 (in Russ.)

18. Turygin V.V., Tomilov A.P. Electrochemical synthesis of triethylphosphate from white phosphorus. Himicheskaia tekhnologiia [Chemical Technology], 2005, no.5, pp. 9-16 (in Russ.)

19. Tomilov A.P. Rational technological environment of the process of electrosynthesis of organic compounds. Himicheskaia promyshlennost [Chemical Industry], 1978, no. 8, pp. 574- 579 (in Russ.)

20. Smirnov Yu.D., Fedorova L.A., Tomilov A.P. Advanced electrochemical synthesis of *p*-chloroaniline. Elektrohimiia [Elecnrochemistry], 1987, T. 33, № 10, pp. 1257 – 1261 (in Russ.)

21. Tomilov A.P., Smirnov Yu.D. Electrolysis of two-phase systems – perspective direction of technological environment of electrochemical synthesis of organic compounds. Himicheskaia promyshlennost [Chemical Industry], 1990, no. 7, pp. 387- 391 (in Russ.)

22. Fioshin M.Ya., Tomilov A.P. Industrial electrolyzers for synthesis of organice compounds. Himicheskaia promyshlennost [Chemical Industry], 1968, no.2, pp. 84-91(in Russ.)

23. Tomilov A.P. Electrochemical syntheses in anhydrous alcohols. Elektrohimiia [Electrochemistry ], 2000. v. 36. no. 2. pp. 118-122 (in Russ.)

24. Ilovaiskii A.I., Merkulova V.M., Elinson M.M., Nikishin G.I. Electrochemical dimerization of dinitrileacetonitriles. V kn.: Novosti elektrohimii organicheskikh soedinenii. Tezisy docladov XVII soveshchaniya [In book: News of Electrochemistry of Organic compounds. Heads of reports XVII conference], Tambov GOU TGTU, 2010, p. 109 (in Russ.)

25. Tomilov A.P. Electrochemical syntheses with sacrificial anodes. Elektrohimiia [Electrochemistry], 1996, v. 32, no. 1, pp. 30-41 (in Russ.)

26. Merkulova V.M., Ilovaiskii A.I., Elinson M.M., Nikishin G.I. Electrochemically initiated chain process: aldol reactions with the participation of izatins and pyrazolones. V kn.: Novosti elektrohimii organicheskikh soedinenii. Tezisy docladov XVII soveshchaniya [In book: News of Electrochemical of Organic compounds. Heads of reports XVII conference], Tambov GOU TGTU, 2010, p. 116 (in Russ.)

27. Merkulova V.M., Ilovaiskii A.I., Elinson M.M., Nikishin G.I. Electrocatalytic multicomponent synthesis of 5-aryl-1,3,4,5-tetrahydro-2n-pyrano[2,3-d] pyrimidines. V kn.: Novosti elektrohimii organicheskikh soedinenii. Tezisy docladov XVII soveshchaniya [In book: News of Electrochemical of Organic compounds. Heads of reports XVII conference], Tambov GOU TGTU, 2010, p. 117 (in Russ.).

28. Tomilov A.P., Smirnov M.K. Turygin V.V., Hudenko V.V. The use of electrochemical methods in the development of low-waste productions. Himiia v interesakh ustoichivogo razvitiia [Chemistry in interests of sustainable development], 2006, v. 14, pp. 175-179 (in Russ.).

**Poly(arylene sulfide)s on the dinuclear aromatic hydrocarbons and sulfur basis**

**Lyubov Alexandrovna Korneeva**

National Research University “MPEI”. Senior Lecturer, Department of Chemistry and Electric-Chemical Energetic Division, Institute of Power Engineering Efficiency Problems.

Krasnokazarmennaya, 14. Moscow, 111250. Russia.

Tel.: (495) 362-70-31. Е-mail: korneevala@bk.ru

**Boris Alexandrovich Zachernyuk**

K.G. Razumovski Moscow State University of Technologies and Management (The First Cossack University). Ph.D., associate professor, Inorganic and analytical chemistry named after Y. A. Klyachko Division.

Ground Shaft, 73. Moscow, 109004. Russia.

Tel.: (499) 236-71-60. Е-mail: zachern@rambler.ru

**Vladimir Ivanovich Nedel’kin**

K.G. Razumovski Moscow State University of Technologies and Management (The First Cossack University).

Ph.D., Professor, Head of the Department, Inorganic and analytical chemistry named after Y. A. Klyachko Division.

Ground Shaft, 73. Moscow, 109004. Russia.

Tel.: (499) 236-72-95. Е-mail: vinedelkin@mail.ru

**Keywords**:polycondensation, poly(arylene sulfide)s, electrophilic substitution, aluminum chloride, elementary sulfur, dinuclear aromatic hydrocarbons, thianthrene.

The poly(arylene sulfide)s of different structures were synthesized by the high-temperature interaction of the sulfur dinuclear aromatic hydrocarbons (diphenyle, diphenylsulfide, diphenyldisulfide and diphenylamine) with elementary sulfur in the presence of AlCl3. It was found that the electrophilic tiiliration of the aromatic nucleus of these compaunds proceeds through the intermediate formation of the intramolecular cyclic arylene sulfides. By IR-, NMR-spectroscopy, mass-spectrometry showed that the tiiliration of dinuclear arenes already having sulfide or disulfide bridges, forming the ring-chain structure polymers with thianthrene sulfide groups and the polimerformation proceeds due to the homopolycondensation of aromatic sulfide under the influence of AlCl3. And the tiiliration of arenes without sulphide bridges leads to the poly(arylene sulfide)s with a predominant content of the *ortho*-phenylene fragments in the chain.

**References**

1. Zachernyuk B.A., Savin E.D., Nedel'Kin V.I. Recent advances [in the chemistry of sulfur-containing poly(arylenes).](http://elibrary.ru/item.asp?id=18251897) [Polymer Science. Series C](http://elibrary.ru/contents.asp?issueid=1076751), 2002, vol. 44, no. 2, pp. 168–184.

2. *Nedel'Kin V.I.*, *Zachernyuk B.A., Andrianova О.B*. Organic polymers based on elemental sulfur and its simplest compounds. Rosiyskiy himicheskiy zhurnal [Russian Chemical Journal], 2005, vol. 49, no. 6, pp. 3-10 (in Russ.).

3. *Korneeva L.A.,* *Zachernyuk B.A*., *Nedel'Kin V.I.* Synthesis and properties of olygo(arylene sulfide)s – products of polycondensation replaced arenes with elementary sulfur**.** Estestvennie i tehnicheskie nauki[Natural and Technical Sciences], 2011, no.2, pp. 58–60 (in Russ.).

4. Vasilkov A.Y., *Zachernyuk B.A*., *Nedel'Kin V.I.* etc. Magnetic and dielectric composite materials on the basis of functional poly(phenylene sulfide)s that contain nanoparticles of iron. Zhurnal prikladnoy himii [Journal of Applied Chemistry], 2007, vol. 80, no. 12, pp. 2058-2062 (in Russ.).

5. Pramanik P., Mukerjee D. An organic Semiconducting polymer containing sulphur bridges. Indian J. Chem. Section A, 1983, vol. 22, no. 1, pp. 44-45.

6. Chemist directory. 3 ed.,vol. 2, L.: Chemistry, 1971,1168 p. (in Russ.).

7. Сhemist's quick reference. Kiev: Publ. H. of AS USSR, 1962, 659 p. (in Russ.).

**Hot-melt fluid bed granulation is alternative to fluid bed coating**

**Gordienko Mariia Gennadievna**

D.I. Mendeleyev University of Russia

Science-research department

125480, Moscow, 20 Geroev Panfilovtsev str., off. 323

**Sinitsa Evgenia Alexandrovna**

D.I. Mendeleyev University of Russia

Computer aided engineering department

125480, Moscow, 20 Geroev Panfilovtsev str., off. 241

**Menshutina Natalia Vasilievna**

D.I. Mendeleyev University of Russia

International Science and Education Center for Transfer of Biopharmaceutical technologies

125480, Moscow, 20 Geroev Panfilovtsev str., off. 241

**Keywords:** hot-melt granulation, fluid-bed, film coating, drug release kinetic.

The hot-melt fluid bed granulation as well as fluid bed coating allowed to produce the drug with sustained release. The defined composition of emulsion self-emulsified during dissolution test. Significant differences in the API release kinetic between the sample obtained by hot-melt granulation and a sample obtained by coating are absent for the first 30 min. During the next 30 min the dissolution profiles vary significantly, while the sample prepared by hot-melt granulation has a greater sustained release effect. It was noted that using a hot-melt granulation time costs are reduced by 3-3.5 times. The hot-melt granulation does not require heating of the fluidizing air.

**References**

1. Mishina Yu.V., Menshutina N.V. Technologies and equipment for production of solid dosage forms. M.: RHTU im. D.I. Mendeleyev [Moscow: MUCTR], 2010 (in Russ).

2. Murav’ev I.A. Technology dosage forms: the textbook for students of pharmacy schools. М.: Medicina [Moscow: Medcine], 1988 (in Russ).

3. Gavin M. Walker, Clive R. Holland, Mohammad M.N. Ahmad, Duncan Q.M. Craig. Influence of process parameters of fluidized hot-melt granulation and tablet pressing of pharmaceutical powders. Chemical Engineering Science, 2005, V. 60, no. 14, pp. 3867-3877.

4. Walker G.M., Bell S.E.J., Andrews G., Jones D.. Co-melt fluidized bed granulation of pharmaceutical powders: Improvements in drug bioavailability. Chemical Engineering Science, 2007, V. 62, no. 1-2, pp. 451-462.

5. Kowalski J., Kalb O., Joshi Y.M., Serajuddin A.T.M.. Application of melt granulation technology to enhance stability of a moisture sensitive immediate-release drug product. International Journal of Pharmaceutics, 2009, V. 381, no. 1, pp. 56-61.

6. Shiino K., Iwao Y., Fujinami Y., Itai S. Preparation and evolution of granules with pH-dependent release by melt granulation. International Journal of Pharmaceutics, 2012, V. 431, no. 1-2, pp. 70-77.