Industrial experience of 70% hydrofluoric acid rectification

Volosnyev Aleksander V., JSC "Leading Research Institute of Chemical Technology", a leading researcher in the Department "Nuclear materials". Address: 115409, Moscow, Kashirsky highway, 33; tel. +7-499-324 - 8869.

Gromov Oleg B., JSC "Leading Research Institute of Chemical Technology", Dr., Head of the Department "Nuclear materials". Address: 115409, Moscow, Kashirsky highway, 33; tel. 8-499-324-8869; fax 8-499-324-5441 (for Gromov O.B.); e-mail: gromov@vniiht.ru; ollgromov@mail.ru

Seredenko Viktor A., JSC "Leading Research Institute of Chemical Technology", PhDr., director of the adviser. Address: 115409, Moscow, Kashirsky highway,  33; tel. +7-499-324-4050.

Skorynin Gennadiy M., JSC "Production Association" Electrochemical Plant ", Dr., Advisor to the General Director for Science, 663690, Russia, Krasnoyarsk terr., Zelenogorsk, st. First Industrial, 1, tel. + 7-39169-9-4040; fax + 7-39169-3-3347.

Andreev Sergey A., JSC "Production Association" Electrochemical Plant ", head of production processing of depleted uranium hexafluoride, 663690, Russia, Krasnoyarsk terr., Zelenogorsk, st. First Industrial, 1, tel. +7-39169-4-9902.

Kuliev Rustam U., JSC "Production Association" Electrochemical Plant ", the chief engineer of the production processing of depleted uranium hexafluoride, 663690, Russia, Krasnoyarsk terr., Zelenogorsk, st. First Industrial, 1, tel. +7-39169-9-3300.

Dolgov Sergey A., JSC "Production Association" Electrochemical Plant ", Head of the research laboratory, 663690, Russia, Krasnoyarsk terr., Zelenogorsk, st. First Industrial, 1, tel. +7-39169-9-3150, fax +7 39169-9-4529.

Tochilin Sergey B., JSC " Siberian group Chemical Industries ", director of the Siberian group, 636,030, Seversk Tomsk region, St. Kurchatov, 1, tel. +7-382-354-8523.

Smagin Aleksander A., JSC " Siberian group Chemical Industries ", a research engineer of the Central plant laboratory, 636030, Seversk Tomsk region., St. Kurchatov, 1, tel. +7-382-354-3361.

Krutyh Viktor N., JSC " Siberian group Chemical Industries ", Dr., technical director of the Siberian group, 636,030, Seversk Tomsk region, St. Kurchatov, 1, tel. +7-382-354-8523.

Skotnov Aleksander S., JSC " Siberian group Chemical Industries ", a research engineer of the Central plant laboratory, 636030, Seversk Tomsk region., St. Kurchatov, 1, tel. +7-382-354-3361.

Keywords: depleted uranium hexafluoride, hydrofluoric acid, rectification, anhydrous hydrogen fluoride, composition, quality.

In JSC “ECP” conversion of the uranium hexafluoride impoverished on isotope 235U – potentially hazardous substance, - is conducted on the W-ECP installation with production of uranium oxides and 70% hydrofluoric acid which converted processin of the further rectification to a anhydrous hydrogen fluoride and 40% hydrofluoric acid. It is shown that quality of a anhydrous hydrogen fluoride conforms to the standard. Owing to strong corrosion of the reactor during pyrohydrolysis of uranium hexafluoride at temperature up to 930 °C the liquid products contain impurities which limits use of acids in a nuclear fuel cycle, but doesn't prevent their application in other branches. The content of uranium in the hydrofluoric acids and anhydrous HF received on the W-ECP installation doesn't exceed 5 ppm what is the level of a similar of JSC “Halogen”.

References

1. Shatalov V.V., Seredenko V.A., Gromov O.B. et al. Depleted uranium hexafluoride – The fluorine source for production of the inorganic and organic compounds. J. Fluor. Chem., v.130, № 1, 2009, pp. 122-126.

2. Volosnyev A.V., Gromov O.B., Frolkina V.V., Reznikova T.E. // In "Proceeding of scientific-practical conference, dedicated to the 105th anniversary of B.V. Gromov. Tomsk, 1-3 October 2014" - Tomsk: Publishing house TPU, 2014. p. 36. (in Russ.).

3. Andriets S.P., Smagin A.A., Gushchin A.A. et al. // In "Abstracts of the All-Russian scientific-practical conference" Fluoride Technologies ", Tomsk, 25-26 June 2009" - Tomsk: TPU, 2009, p. 13. (in Russ.).

4. Volosnyev A.V., Gromov O.B., Medvedev M.V. et al. A process for preparing anhydrous hydrogen fluoride and hydrofluoric acid. RU 2447013, 2012. (in Russ.).

5. Volosnyev A.V., Gromov O.B., Seredenko V.A. et al. Optimal reactor structural material for the fluorination of uranium oxides by gaseous hydrogen fluoride. Atomnaya energiya [Atomic energy], v. 114, № 5, 2013, pp. 285-288. (in Russ.).

6. Gromov B.V. Introduction to the chemical uranium technology. // M .: Atomizdat, 1978, pp. 32, 33. (in Russ.).

Determination peculiarities of complex mineral fertilizers phase composition

Kochetova Inna, The Research Institute for Mineral Fertilizers (JSC «NIUIF»), researcher; e-mail: inna_kocetova@mail.ru

Sokolov  Valery, Ph.D., The Research Institute for Mineral Fertilizers (NIUIF)

Mihaylichenko Anatoliy, Doctor of Chemical Sciences, Professor, D. Mendeleev University of Chemical Technology of Russia; e-mail: mikhayl@muctr.ru

Bakhvalov Alexey, Ph.D., leading specialist, "Scientific instruments" Stock Company (52, Marshala Govorova, Saint-Petersburg, 198095); e-mail: bakhvalov@sinstr.ru

Bakhvalovа Elena, Ph.D., leading specialist, "Scientific instruments" Stock Company (52, Marshala Govorova, Saint-Petersburg, 198095); e-mail: bakhvalova@sinstr.ru

Keywords: complex mineral fertilizers, X-ray diffraction analysis, solid-phase reactions, XRF micro-analysis, X-ray microtomography.

The phase composition and structure of granules of complex mineral fertilizers were intestigated. Modern nondestructive methods of analysis, such as microtomography and the X-ray fluorescent microanalysis, allow to investigate in more detail structure of granules of complex mineral fertilizers.

Investigation of structure and phase composition of granules of NPK fertilizer 15:15:15 was carried out by means of  X-ray microtomograph SkyScan 1172 (Bruker), scanning electronic microscope TM-3030 (HITACHI) with EDS system Quantax-70 (Bruker)  and X-ray fluorescent microscope microprobe RAM-30µ (JSC Nauchnye pribory) It can be concluded from these investigations that conversion reactions in granules don’t occur in considerable scales.

References

1.	Kuvshinnikov I.M. Mineral fertilizers and salts. Properties and ways of their improvement. M.: Chimia, 1987, 256 p. (in Russ.).

2.	Vonk C.G, Heck H.G., Pijpers A.P.. Quantitative X-Ray analysis of crystalline components in fertilizers. New Developments in Phosphate Fertilizer Technology, Proceedings of the 1976 Technical Conference of ISMA LTD, Netherlands, 1976, pp. 115-126.

3.	Bushuev N.N. etc. Research of phase composition of nitrogen-phosphorus-potassium fertilizers of brands (NPK) of brands 8:24:24, 10:20:20, 15:15:15. Mir sery i N P K [World of Sulfur and N P K], 2012, №2, pp.12-19 (in Russ.).

4.	Bushuev N.N., Norov A.M., Lobacheva M.P. etc. Phase composition of nitrogen-phosphorus-potassium fertilizer of brand 8:24:24 and sulfoammophos (NP+S) brand 15:36+9. Mir sery i N P K [World of Sulfur and N P K], 2011, №4, pp. 16-23 (in Russ.).

5.	Gavin M. Walker, T. Ronald A. Magee, Clive R Holland. Caking processes in granular NPK fertilizers. Ind. Eng. Chem. Res., 1998, vol. 37, pp. 435-438

6.	Kuznecova G.L. Qualitative x-ray analysis. Irkutsk, IGU, 2005, 28 p. (in Russ.).

7.	Kovba L.M., Trunov V.K. X-ray analysis. Moscow, MGU, 1976,  232 p. (in Russ.).

8.	Eric N. Landis, Denis T. Keane. X-ray microtomography. Materials Characterization, 2010, Vol. 61. Issue 12, pp. 1305-1316.

9.	Kochetova I.M. etc. Methods of research of structure of mineral fertilizers granules. Materialy seminara «Rol' analiticheskih sluzhb v obespechenii kachestva mineral'nyh udobrenij i sernoj kisloty». [Seminar materials "Role of analytical services in quality assurance of mineral fertilizers and sulfuric acid"], Moscow, NIUIF, 2015, pp. 42-49 (in Russ.).

10.	B. Scruggs, M. Haaske, L. Herczeg, J. Nicolosi. XRF mapping: new tools for distribution analysis.  Advances in X-ray Analysis. 2000, V. 42, pp. 19-25.

11.	Bahvalov A.S., Volkov P.G., Chizhova E.V. Obtaining of continuous distribution of elements by method of the X-ray fluorescent microanalysis. V mire nauchnyh otkrytij [In the world of discoveries], 2010. № 2 (08). vol. 3. pp. 19-20 (in Russ.).

12.	Chizhova E.V. Modeling of X-ray fluorescent microanalyzer operation, assessment of analytical and metrological parameters. Nauchnoe priborostroenie [Scientific instrument making], 2012. vol. 22, № 2. pp. 55-65 (in Russ.).

Resource-saving technology of electroless Nickel plating

Vinokurov Evgeniy G., Doctor of Chemical Science, professor,  D.Mendeleev University of Chemical Technology of Russia, Moscow; e-mail: vin-62@mail.ru

Skopintsev Vladimir D., Ph.D., Senior researcher, D.Mendeleev University of Chemical Technology of Russia, Moscow; e-mail: scopintsev@yandex.ru

Nevmyatullina Hadiya A., Candidate of engineering sciences, Associate professor of D. Mendeleyev University of Chemical Technology of Russia; e-mail: knevm@mail.ru.

Morgunov Andrey V., assistant,  Russian state agrarian University – MTAA named after K. A. Timiryazev; e-mail: morgunovand@mail.ru.

Keywords: electroless Nickel plating, Nickel-copper-phosphorus alloy, deposition rate, stable solution.

Introduction to electroless Nickel plating electrolyte glycine and malonic acid as ligands and Pb2+ and Cu2+ as stabilizers increases the stability of the solution, duration of use and deposition rate of coatings. The experiments allow to develop a stable solution for obtaining Nickel-phosphorus coatings doped with copper, with high performance. Tested methods of periodic and continuous correction of electrolyte and removal of accumulated components allow to maintain the optimum composition of the solution during prolonged use and to reduce the specific consumption of reagents in the deposition of coatings.

References

1. Gorbunova K.M., Ivanov M.V., Galvanotechnics. M. : Metallurgia,1987. 736 p. (In Russ.).

2. Norkus P.K., Markyavichene R.M. Separate titrimetric determination of hypophosphite and phosphite. Zhurnal analiticheskoy khimii [Journal of analytic chemistry], 1967, no. 10, pp. 1527 – 1530 (In Russ.).

3. Kotik F.I. Accelerated control of electrolytes, solutions and melts. М.:  Мashinostroenie, 1978. 102 p. (In Russ.).

4. GOST 9.305–84 Coating metallic and non-metallic inorganic. Operations of technological processes of coating obtaining. M.: Izdatelstvo standartov, 2003. 106 p. (In Russ.).

5. Morgunov A.V., Skopintsev V.D. Electrolytic deposition of Nickel-phosphorus coatings doped with copper. Galvanotehnika i obrabotka poverhnosti        [Electroplating and surface treatment], 2008, no. 3, pp. 30-34 (In Russ.).

6. Vinokurov E.G., Zhigunov F.N., Morgunov A.V., Skopintsev V.D. Electrolytic deposition of  Nickel-phosphorus and Nickel-phosphorus-copper coatings from  glycinate solutions. Galvanotehnika i obrabotka poverhnosti        [Electroplating and surface treatment], 2015, no. 3, pp. 40-46 (In Russ.).

7.    Gokzhaev M.B., Morgunov A.V., Skopintsev V.D. Optimizing solution composition for the chemical deposition of Nickel- copper-phosphorus alloys.  Inorganic Materials, 2008, no. 12, pp. 1319-1321. (In Russ.).

Theoretical optimization of catalytic processes on the basis of economic criteria

Koledin Sergey Nikolaevich

Institute of Petrochemistry and Catalysis of RAS, post-graduate student

Address: 450075, Russia, Republic of Bashkortostan, Ufa, October Prospect, 141;

e-mail: koledinsrg@gmail.com

Koledina Kamila Feliksovna

Institute of Petrochemistry and Catalysis of RAS, Research Associate

Ufa State Petroleum Technological University, Associate Professor

Address: 450075, Russia, Republic of Bashkortostan, Ufa, October Prospect, 141;

e-mail: koledinakamila@mail.ru

Gubaidullin Irek Marsovich

Institute of Petrochemistry and Catalysis of RAS, senior researcher

Ufa State Petroleum Technological University, Professor

Address: 450075, Russia, Republic of Bashkortostan, Ufa, October Prospect, 141;

e-mail: irekmars@mail.ru

Spivak Semyon Izrailevich

Institute of Petrochemistry and Catalysis of RAS, Head. Laboratory of Mathematical Chemistry, Bashkir State University, Professor, Head. Department of Mathematical Modeling. Address: 450075, Russia, Republic of Bashkortostan, Ufa, October Prospect, 141; e-mail: semen.spivak@mail.ru

## Keywords: theoretical optimization, economic criteria, the kinetic model of the reaction of alcohols with dimethyl carbonate, green chemistry.

A kinetic model of catalytic reaction of alcohols with dimethyl carbonate was developed, the rate constants and energy activation of stages were determined. Kinetic parameters of experiments with different initial concentrations of the catalyst were analyzed. As the criteria for the solution of the taskof process optimisatien the productivity and profitability of the process were choosen.The eguations received were used for calcubation of the conditions for achieving the extreme values of the indicators. It is shown that the highest possible conversion of the starting reagent dols not give economically optimal solution. Calculations of the dependence of the criteria of optimality on the process parameters malles it possible to determine the optimal conditions to maximize productivity and profitability in the investigated range of parameters.

References

1. Slin'ko M.G. History of the development of mathematical modeling of catalytic processes and reactors .// Teoreticheskie osnovyi himicheskoy tehnologii [Theoretical Foundations of Chemical Technology], 2007, volume 41, no 1, pp 16-34. (in Russ.).

2. Slin'ko M.G. Fundamentals and principles of mathematical modeling of catalytic processes. // Novosibirsk: IK SO RAN, 2004. (in Russ.).

3. Boyarinov A.I., Gafarov V.V. Optimization methods in chemical technology. // М.: Chimia, 1975. (in Russ.).

4. Bykov V.I. Direct and inverse problems of chemical kinetics.//Nauka, Novosibirsk, 1993. (in Russ.).

5. Golovanchikov A.B., Dulkina N.A., Aristova Yu.V.  Mathematical modeling of chemical reactors with different structures streams in the source component and the reaction product // Himicheskaya promyishlennost segodnya[Chemical Industry Today], 2014, №9, pp. 28-34 (in Russ.).

6. Pisarev M.O., Dolganov I.M., Ivashkina E.N., Dmitriev A.Yu. Improving the efficiency of technological devices installation of low-temperature gas separation using a simulation of the dynamic model // Himicheskaya promyishlennost segodnya[Chemical Industry Today], 2016, №5, pp. 45-56 (in Russ.).

7. Mustafina S., Mikhailova T., Mustafin T. Optimal parameters of the α-methylstyrene oligomerization reaction in the presence of a zeolite catalyst.//

International Journal of Chemical Sciences, 2015, T. 13, № 2, pp. 1071-1075.

8. Zhukov D.Y. Simulation and Optimization of sorption process of a manganese precipitate containing manganese carbonate. // Himicheskaya promyishlennost segodnya [Chemical industry today], 2015, № 6, pp 18-25. (in Russ.).

9. Khusnutdinov R.I., Schadneva N.A., Mayakova Y.Y. Synthesis alkilmetilovyh alkilmetilkarbonatov esters by reacting dimethyl carbonate with alcohols in the presence of W and complexes Co.// Zhurnal organicheskoy himii [Russian Journal of Organic Chemistry], 2014, vol 50, no. 6, pp 808-813. (in Russ.).

10. Tundo P. New developments in dimethylcarbonate chemistry // Pure and Applied Chemistry, 2001, V.73, P. 1117-1120.

11. Koledina K.F., Gubaidullin I.M. Kinetics and mechanism of catalytic reactions of olefins hydroaluminizing organoaluminum compounds.// Zhurnal fizicheskoy himii [Journal of Physical Chemistry], 2016, volume 90, number 5, pp 673-680. (in Russ.).

12. Koledin S.N., Koledina K.F. Planning economically optimal chemical experiment based on the kinetic model of catalytic reaction of alcohols with dimethyl carbonate.// Zhurnal Srednevolzhskogo matematicheskogo obschestva [Journal Srednevolzhsky Mathematical Society], 2015, Volume 17, number 2, pp 43-50. (in Russ.).

13. Manish Kaushika, Ayodhya Singhb, Munesh Kumara. The chemistry of group-VIb metal carbonyls.// European Journal of Chemistry, 3 (3), 2012, pp.367-394.

14. Koledina K.F., Gubaidullin I.M. The software package for the solution of inverse problems of chemical kinetics and its realization in a virtual test bed .// Nauka i obrazovanie: Nauchnoe izdanie MGTU im. N.E. Baumana [Education & Science: Scientific publication MSTU. N.E. Bauman], 2013, number 7, pp 385-398. (in Russ.).

15. Turanyi T, Nagy T, Zsely IGy, Cserhati M, Varga T, Szabo BT, Sedyo I, Kiss PT, Zempleni A, Curran HJ Determination of rate parameters based on both direct and indirect measurements // International Journal of Chemical Kinetics, 2012, 44 (5), P. 284-302

16. Alshin A.B., Alshina A.E., Kalitkin N.N., Koriagina A.B. Rosenbrock schemes with complex coefficients for stiff and differential-algebraic systems.// Zhurnal vyichislitelnoy matematiki i matematicheskoy fiziki [Computational Mathematics and Mathematical Physics], 2006, v. 46, no 8, pp. 1392-1414. (in Russ.).

17. Gubaydullin I.M., Koledina K.F., Sayfullina L.V. Mathematical Modeling of Induction Period of the Olefins Hydroalumination Reaction by Diisobutylaluminiumchloride Catalyzed with Cp2ZrCl.//Engineering Journal, 2014, T. 18, № 1, P. 13.

18. Goldberg D.E.  Genetic algorithms in search, optimization, and machine learning //  Addison-Wesley, USA, 1989.

19. Novichkova A.V., Bobrenёva J.O., Gubaidullin I.M., Koledina K.F. The program of calculation of uncertainty bands kinetic parameters «INTKIN». The certificate of registration of an electronic resource number 19951 on February 24, 2014 AS 19951 Russian Federation // The combined fund of electronic resources Chronicle Science and Education, 2014, volume 1, number 2 (57), S. 52. (in Russ.).

20. Gubaidullin IM, Koledina KF, Lind YB Modern technologies of high performance computing for modeling the detailed mechanism of the catalytic reaction hydroaluminizing olefins. // Education & Science: Scientific publication MSTU. NE Bauman [Education & Science: Scientific publication MSTU. NE Bauman], 2011, № 6, S. 10. (in Russ.).

21. Gubaidullin I.M., Koledina K.F., Spivak S.I. Sectors Structural and parametric identification of kinetic models of chemical reactions involving organometallic compounds based on information and computer analysis system.// Himicheskaya promyishlennost segodnya [Chemical industry today], 2014, number 11, C. 18-27. (in Russ.).

22. Nurislamova L. F., Gubaydullin I. M., Koledina K.F. Kinetic model of isolated reactions of the catalytic hydroalumination of olefins.// Reaction Kinetics, Mechanisms and Catalysis, 2015, volume 116, issue 1, pp. 79-93.

23. Kramers H., Vestreterp K. Chemical reactors. Calculation and management. // М.: Chimia, 1967, C.264. (in Russ.).

Laboratory research and pilot testing of heat exchangers for heating dissolve lye

Kalishuk Dmitry Grigorievich

Belarusian State Technological University, Department of Processes and Apparatus of Chemical Production, Ph. D. Engineering, Associate Professor

13a, Sverdlova str., Minsk, 220006, Republic of Belarus

Тел. раб. +375(17)226-00-39

e-mail: kalishdz@belstu.by

Saevitch Nikolay Petrovich

Belarusian State Technological University, Department of Processes and Apparatus of Chemical Production, Ph. D. Engineering, Associate Professor

13a, Sverdlova str., Minsk, 220006, Republic of Belarus

Тел. раб. +375(17)226-00-39

e-mail: saevichm@belstu.by

Levdansky Alexander Eduardovich

Belarusian State Technological University, Department of Processes and Apparatus of Chemical Production, Grand Ph. D. Engineering, Associate Professor

13a, Sverdlova str., Minsk, 220006, Republic of Belarus

Тел. раб. +375(17)226-00-39

e-mail: alex_levdansky@belstu.by

Chirkun Dmitry Ivanovich

Belarusian State Technological University, Department of Processes and Apparatus of Chemical Production, Ph. D. Engineering, senior lecturer

13a, Sverdlova str., Minsk, 220006, Republic of Belarus

Тел. раб. +375(17)226-00-39

e-mail: chirkund@gmail.com

Opimah EevgenyVladimirovich

Belarusian State Technological University, Department of Processes and Apparatus of Chemical Production, graduate

13a, Sverdlova str., Minsk, 220006, Republic of Belarus

Тел. раб. +375(17)226-00-39

e-mail: opimah.evgenij@belstu.by

Keywords: heat exchanger, mixing, direct steam, jet apparatus, liquid, dissolving liquid lye, potassium chloride.

The article proved the possibility of jet mixing heat exchangers for stabilizing the temperature in a solvent sylvinite ore. We analyzed different designs of jet heat exchangers and identified the most suitable for use in potash technology. A laboratory installation for studying the circulation was created and capacitive jet heat exchangers, a brief description of the studied modifications of devices were given. The results of experimental research, experimental data treatment and their analysis were presented. It sets out details of the thermal characteristics and operating conditions tested models. The possibility of application apparatus designed on the basis of laboratory tests, for heating in a solvent medium sylvinite ores and stabilize its temperature. The results of pilot tests of the jet heat exchanger "vapor-liquid" on the stage of dissolution were presented.

References

1.	Pechkovskiy V.V. Potash fertilizer technology. Minsk: Vysheysh. shkola, 1968. 264 p. (in Russ.).

2.	Aksel'rud G.A., Molchanov A.D. Dissolving solids. M.: Chimia, 1977. 272 p. (in Russ.).

3.	Kasatkin A.G. Basic processes and apparatuses of chemical technology. M.: Al'yans, 2004. 753 p. (in Russ.).

4.	Lukanin V.N., Shatrov M.G., Kamfer G.M. i dr. Heat engineering: textbook for High Schools. M.: Vyssh. shk., 2000. 671 p. (in Russ.).

5.	Isachenko V.P., Osipova V.A., Sukomel A.S. Heat transfer. M.: Energoatomizdat, 1981. 415 p. (in Russ.).

6.	Ermolov V.F., Permyakov V.A., Efimochkin G.I., Verbitskiy V.L. Mixing heaters of steam turbines. M.: Energoizdat, 1982. 208 p. (in Russ.).

7.	Taubman E.I., Gornev V.A., Mel'tser V.L. i dr. Contact heat exchangers. M.: Chimia, 1988. 256 p. (in Russ.).

8.	Sokolov E.Ya., Zinger N.M. Inkjet devices. M.: Energoatomizdat, 1989. 352 p. (in Russ.).

9.	Tsegel'skiy V.G. Two-phase jet devices. M.: Izd-vo MGTU im. N.E. Baumana, 2003. 408 p. (in Russ.).

10.	Sosnin Yu.P. Contact water heaters. M.: Stroyizdat, 1974. 359 p. (in Russ.).

11.	Belevich A.I., Kruptsev A.V., Malofeev V.A. On the application of heat in a heat supply injectors. Energetik [Energetik], 2001, no.11. pp. 20–22 (in Russ.).

12.	Nedugov A.F., Kurkulov M.A. Water-jet steam ejector camera premix. Promyshlennaya energetika [Industrial power], 2007, no.1. pp. 20–23 (in Russ.).

13.	Product catalog Spirax Sarco (www. Spiraxsarco.com/ru).

Computer-aided design for technological pipelines heating by heat tracers

Kokhov Timur Aleksandrovich, JSC "Giprogazoochistka", Engineer CAD Department, 126, Pervomayskaya St., Moscow, 105203, Russian Chemical-Technological Mendeleev University, Postgraduate, tel. (495) 231-30-52 (ext. 4851); e-mail: tkohov@ggo.ru.

Keywords: Technological pipelines, Heat tracing, Heating contour, Automated Information System (AIS), Computer-aided design (CAD), Software package, 3D-design, AVEVA Engineering, AVEVA PDMS, 1Insulation.

Currently 70% of the industrial facilities are still heated by steam. Steam tracing systems have been successfully used worldwide to improve efficiency in the petrochemical, process industry, power plants and other strategic industries. Steam heating solutions designed to generate and maintain the temperature for all modes of freeze protection to high temperature process control. The advantage of the approach developed for the implementation of the programs of calculation and design of technological piping heating to existing systems is that they are integrated into a system of computer-aided design AVEVA PDMS, AVEVA Engineering design data management system and synchronized with the program for the design of heat-insulating structures "Isolation".

References

1.	Magalif V.Y., Itkina D.M., Korelshteyn L.B. Installation design of chemical, petrochemical and refining industries, Moscow, Navigator [The Navigator], 2010 – 344 p. (in Russ).

2.	Khizhnyakov S.V. Practical calculations of thermal insulation, Moscow, Jenergija [ENERGY], 1976 – 145 p.

3.	Mirkin A.Z., Usinsh V.V. Pipeline Systems: Ref. Ed. – Moscow, Himija [Chemistry], 1991 – 256 p. (in Russ).

4.	Guriev V.V., Acorn V.S., Petrov-Denisov V.G. Thermal insulation in the industry. The theory and calculation, Moscow, Strojizdat [Stroyizdat] 2003 – 416 p. (in Russ).

5.	J. PHILLIP ELLENBERGER. Piping and Pipeline Calculations Manual Construction, Design Fabrication and Examination. Second Edition. USA, Elsevier, 2014 – 398p.

6.	Mohinder L. Nayyar. Piping handbook. 7th ed. USA, McGraw-Hill, 2000 – 2482 p.

7.	Thermon Manufacturing Company | The Heat Tracing Specialist (http://www.thermon.ru/).

8.	Luke M.A., Mizerls K.K., "Comparison of steam and heating plant at work», Oil and Gas Journal, November 1977, p. 64-73.

9.	Gartman T.N., Sovetin F.S., Novikov D.K. Development of a computer model of a multi-stage production of methanol from natural gas. Himicheskaja promyshlennost' segodnja [Chemical industry today], no.3. 2012. p. 45-53. (in Russ).

10.	Borovkova E.A., Sovetin F.S., Ramazanov A., Gartman T.N. Development of energy-efficient subsystems rectification in the production of aromatic hydrocarbons from light alkanes. Himicheskaja promyshlennost' segodnja [Chemical industry today], no. 8, 2015, p. 39- 50. (in Russ).

11.	Standards. STO PPI / STP 17-02-2010. Heated satellites technological pipelines. The main provisions of the design. Moscow, 2010 – 21 p. (in Russ).

12.	VSN 2-82. Guidelines for the design of industrial pipelines of heating systems and equipment on the open areas in the chemical industry, Moscow, Minhimprom [Minhimprom] 1982 – 25 p. (in Russ).

13.	T-TT-06-85. Album of drawings of the internal facial features. Satellites technological pipelines 1985 – 48p. (in Russ).

14.	VSN 168-76 / MMSS USSR. Instructions for calculation and design of thermal insulation designs product lines, heated steam and water satellites, Moscow, 1978 – 89 p. (in Russ).

15.	Kokhov T.A., Korelshteyn L.B., Gartman T.N. «The software design package for  technological pipelines heating by heat tracers in computer-aided design systems» Programmnye produkty I sistemy [SOFTWARE & SYSTEMS], no. 4 (112), 2015, Tver, 244–248 p.). (in Russ).

16.	The calculation and selection of heat insulation of piping and equipment. User guide. Moscow, 2014 – 280 p.

Theoretical and experimental method for evaluating the territorial air pollution chemical parameters of objects

Kantyukov Rafkat, Ph.D., General Director of "Gazprom Transgaz Kazan." Contact information: telephone number (office) 8 (843) 2726002,
e-mail: info@tattg.gazprom.ru postal address: 420073, Republic of Tatarstan, Kazan,  st. Adel Kuta d. 41.

Meshalkin Valery, Doctor of Technical Sciences, Professor, Director of MI-LRTI, Head of the Department of Logistics and Economic Informatics D. Mendeleev University of Chemical Technology of Russia. Contact information: Phone: 8 (499) 9788923, Fax: 8 (499) 9783164, E-mail: clogist@мuсtr.ru, postal address: 125047, Moscow A-47, Miusskaya Sq., 9 (1st Street Miusskaya . 3).

Panarin Vladimir, Doctor of Technical Sciences, Professor, General Director of "Patent at Tula State University." Contact information: Phone: 8 (4872) 353550, E-mail: panarin-tsu@yandex.ru, postal address 300012, Tula, pr. Lenina 92.

Goryunkova Anna, Doctor of Technical Sciences, assistant professor of Aerology, health and environment of the Tula State University Contact information: Phone: 8 (4872) 353760, E-mail: anna_zuykova@rambler.ru, postal address 300012 , Tula, pr. Lenina 92.

Kantyukov Rafael, Ph.D., deputy chief engineer for operation of the main gas pipelines of "Gazprom Transgaz Kazan." Contact information: telephone number (office) 8 (843) 2728382, e-mail: r-kantyukov@tattg.gazprom.ru, postal address: 420073, Republic of Tatarstan, Kazan, ul. Adel Kuta d. 41.

Grishakov Kirill, graduate student of Aerology, health and environment of the Tula State University Contact information: Phone: 8 (4872) 353760, E-mail: grishakoff.kirill@yandex.ru, postal address 300012 , Tula, pr. Lenina 92.

Keywords: automated system, environmental monitoring, pollution, environment.

Proposed theoretical and experimental method, which solves the problem of the application of a mathematical model to simulate the scattering of pollutants in the atmospheric surface layer in order to reduce the error of the results and the appropriate use of mathematical modeling techniques to the specific conditions of a given territory industrialized region. The method is based on an integrated assessment of the error concentrations obtained experimentally determined values (by measurement) and by modeling the processes occurring in the atmosphere. The proposed method and algorithm of its realization will allow to take effective measures for normalization of emissions of the industrial enterprises in the region and to form a subsystem management decision-making in the field of air protection.

References

1. Meshalkin V.P., Butusov O.B., Smotrych S.A., Selskiy B.E. Information system for environmental zoning of air pool in urban areas // Himicheskaya promishlennost segodnya [Chemical Industryte day], 1997, no.4, pp. 263-269 (in Russ.).

2. Meshalkin V.P., Butusov O.B., Selskiy B.E., Smotrych S.A., Stepanov A.M. Computer modeling of the gas emissions of chemical plants based on man-made obstacles flow // Teoreticheskie osnovy himicheskoj tehnologii [Theoretical Foundations of Chemical Engineering], 1999, t. 33, no.1, pp. 79-86 (in Russ.).

3. Panarin V.M., Goryunkova A.A. The automated system of collection and analysis of environmental data on air pollution // Vestnik komp'juternyh i informacionnyh tehnologij [Herald of computer and information technologies], 2013, no.1 (January), pp. 9-11 (in Russ.).

4. Kantyukov R.A., Meshalkin V.P., Panarin V.M., Goryunkova A.A., Gimranov R.K., Rizhenkov I.V., Kantyukov R.R. Information and measuring control system of geographically remote objects in the gas transport sector // Prikladnaja informatika [Applied Informatics], 2015, t.10, no.3 (57), pp. 51-62 (in Russ.).

5. Meshalkin V.P., Panarin V.M., Goryunkova A.A. Computer modeling of air pollution the ruptured pipeline // Jelektronnyj nauchnyj zhurnal «Neftegazovoe delo» [Electronic scientific journal "Oil and gas business"], 2015, no.1, pp. 307-325 (in Russ.).

6. Kantyukov R.A., Gimranov R.K., Rizhenkov I.V., Kantyukov R.R., Meshalkin V.P. Automation of monitoring the state of the system environment // Himicheskaja promyshlennost' segodnja [Chemical industry today], 2015, no.3, pp. 25-32 (in Russ.).